Characterization of Radiation Damage by Deposition of GaN on GaAs

Moussaoui Nafissa *, Bouafia Mohamed *, Djamel Boubetra **

* 1University Ferhat Abbas Setif, Applied Optics Laboratory, 19000  Algeria

Telephone: (213) 62051808; Email: moussaouinassira@gmail.com

** Centre Universitaire Bordj Bou Arréridj, El Annasser 34265, Algeria

Laboratoire des Materiaux et Composants Electroniques

Telephone: (213) 35666547; Email: boubetra@yahoo.fr

Abstract: Radiation damage by reactive magnetron sputtering deposition at low energies is connected with marked changes of optical constants of semiconductors. It will be shown, that using ellipsometry and a special model can provide information about relevant parameter of the amorphization process of GaN/GaAS layer System. The procedure allows the quantification of the radiation damage in the nanometer range and the refractive index of the formed amorphous GaAs. [The Journal of American Science. 2007;3(3):42-46]. (ISSN: 1545-1003).

Keywords: Physical radiation effects ; Ions ; Argon ions ; Ellipsometry; Semiconductors; Gallium arsenide; Gallium nitride; Amorphization.

1. Introduction

Gallium nitride on arsenide alloys is promising for optoelectronic devices working in the visible wavelength zone (Nakamura at.al. 1994; Nakamura, at .al 1996).

It is well known that the amorphization of Semiconductors crystal by ion implantation (Fried at.al., 1992.; Burns at al, 1991; Hu at.al 1991) or by deposition (Teng at al, 2006; Rogozin at.al 2007) is connected with marked changes of the dielectric function wich can be detected with a high sensitivity by ellipsometry.

If spectroscopic ellipsometry is used, it is possible to obtain the dielectric function for an extend wavelength range and to fit a layer model to the experimental data. In this way complex layer consisting of amorphous and crystalline material including voids can be treated (Vedam at.al, 1985).

For a more detailed analysis of ion target-interactions, it is necessary to develop suitable multi-layer model that can be fitted to the experimental data (Hu at al., 1992).

It will be shown in the presented paper, that using special developed model (Bouafia at.al. 2006) and ellipsometric measurements these changes can provide informations about relevant parameters of the amorphization process as the amorphization state and the critical concentration.

2. Model Assumptions

During ion implantation the concentration of the point defects increases as a result of atomic displacements by nuclear collisions, and above an accumulated critical energy density, these defects will relax into an amorphous state. The amorphization dose Da can then be defined as the ion dose required to deposit the critical energy density C. This will be equivalent to the first appearance of an amorphous layer with the thickness d. The expression of the energy density as function of dosis D is given by:

(1)

where t is the GaN thickness and E is the ion Energy.

It will be assumed that the maximum of the damage depth distribution is located not far from the interface GaN/GaAs and the distribution can be approximated by a Gaussian (see Figure 1).This leads to the mathematical description of the maximum energy density  distribution Cmax given by :

(2)

Here, E is the ion impact energy, x is the depth in the substrate, s is the shift of the distribution related to the interface, and ( is the straggling of the damage distribution.

A less damaged transition layer is formed between the amorphous GaAs and the crystalline GaAs. In the following, the later will be treated as an additional amorphous layer with a thickness df, which will be defined by the equivalence of the areas (see Figure 1):

(3)

Figure 1: Energy density distribution in the system layers GaN(a-GaAS(c-GaAs

The energy densities c1-c3(x) corresponds to different ion dosis. If c(x)>ca the semiconductor substrate is otherwise more or less strongly damaged.

3. Experiment

The GaN films were fabricated by reactive magnetron sputtering in Ar 99,99%-N299,99% gas mixture. A 99,99% purity Ga was used as target. The start pressure was 10-3 Pa. The substrate was located at 50 mm downstream from the target. The films were deposited at 0,6Pa. The partial pressure N2/Ar was 1,75. The substrates used in these experimental work were quartz for transmission measurements and GaAs with (100) orientation (n=2.1017cm-3) for ellipsometric investigations.

GaN/GaAs samples with GaN thicknesses of about 600 nm to 900 nm were implanted with argon ions from a Kaufman-type source with energies from 500eV to 3000eV. GaN layer thickness and ion energy have been adjusted that the maximum of the range distribution was located in the interface GaN/GaAs. The actual value of the ion dose determines the kind of the buried damaged layer (below or above the amorphous threshold, voids) and its extent in the depth.

The ellipsometic measurements were accomplished using rotating analyzer ellipsometer  (Sentech Instruments, Germany) with the fixed laser wavelength 632,8 nm (1,96eV).

The angle of incidence has been chosen to 70° at this angle the laser spot is elliptical with an area of about 6 mm2. Some measurements at other angles were only performed to verify the model.

4. Results and Discussion

Experimental results of optical transmission as function of wavelength of GaN/quartz film with quartz substrate as reference is shown in Figure 2. The interferences maxima in spectra. curves are located very closely.  This indicates that GaN has very high transmission and possess low absorption in the visible a part of the spectrum ((>400 nm). As indicated in Figure 2 the average transmittance of GaN film is about 85%.

Figure 2: Optical transmission of gallium arsenide in dependence on the wavelength

The measuring results of ellipsometry are available in the form of the ellipsometric angles ψ and Δ that are correlated with the amplitude and the phase of the complex reflectance ratio:

where rp and rs are the reflection coefficients of the p- and s-polarized components. The results are shown in Figure 3 in dependence of the GaN layer thickness.

From ψ and Δ values both the thickness and the complex refractive index  of the respective amorphous zone can be derived by fitting model calculations to the measure values. Concerning the amorphization behaviour, the thickness of amorphous GaAs has been found 8 nm. For amorphous GaAs the refractive index value  was an acceptable fit for all values investigated here.

Figure 3: Experimental ellipsometric ψ and Δ curve

This complex refractive index is characterized by comparatively high n and k values compared with crystalline GaAs (), which are typical of amorphous GaAs created by ion damaged (Jellison, 1992) or deposition (Teng at al., 2006). The here found refractive index agrees within some percent with the reported values.

Conclusion

In conclusion, it was the intention of this paper to demonstrate the applicability of the here presented simple procedure to characterize the amorphization of gallium arsenide by low energy, which require otherwise more complex methods.

The method consisting of ellipsometric measurements combined with a model should be applied to determine the depth of the ion implantation damage and the resulting optical properties.

Acknowledgments

The author M. Bouafia gratefully acknowledges the financial support given by the DAAD, Germany.

Correspondence to:

Bouafia Mohamed

Setif University UFAS

Setif 19000. ALGERIA

Telephone: (213) 62051808

Email: bouafiamohamed@gmail.com

References

- Bouafia, M., Moussaoui, N., Boubetra, Dj.,Bouamama, L. and Bouzid, D. 2006, Mathematical modelling of amorphous layers growth by low energy ion implantation, in Proc.Ordre-Désordre Alcane Simulation, OASIS 2006, Bechar, Algeria.

- Burns, T.M., Chongsawangvirod, S., Andrews, J.W., Irene, E.A., Mc.Guire, G. and Chevacharoeukul, S. A. 1991, comparison of the measurement of ion damage in silicon surfaces using differential reflectance and spectroscopic ellipsometry, J. Vac. Sci. Technol. 89: 41.

- Fried M., Lohner T., Aarnink, W.A.M., Hanekamp, L.J. and van Silfhout A-,1992. Nondestructive determination of damage depth profiles in ion-implanted semiconductors by spectroscopic ellipsometry using different optical models, J- Appt. Phys. 71:  2835.

- Jellison, G.E.1992, Jr. Opt. Mater.,  1:151.

- Hu Y-Z-, Li M., Conrad. K, Andrews J.W., Irene, E.A.,  Denker  M., Ray, M. and McGuire G., 1992, In situ spectroscopic  ellipsometry studies of hydrogen ion bombardment of  crystalline   silicon, J.Vac- Sci- Techno, B10: 1111.

- Hu Y.Z., Andrews J-W-, Li M. and IreneE-A-, in situ spectroscopic elipsometric investigation of argon ion bombardment of single-crystal silicon and silicon dioxide films, Nucl. Instrum. Methods, 1991, Phys. Res. 859/60: 76.

- Nakamura, S., Mukai, T.  and Senoh, M. 1994, Appl. Phys. Lett.  64: 1687.

- Nakamura, S., Senoh, M., Nagahama, S.,Iwasa, .Yamada, T., Matsushita,T., Kiyoku, H. and Sugimoto, Y., 1996,  Jpn. J. Appl.   Phys.  35:L74.

- Rogozin, I. V.  and Georgobiani,  A. N.,2007. On the Mechanism of GaN layer growth and defect   formation  in the  GaN-GaAs   system,Bulletin of the Lebedev Physics Institute, 34:114.

- Teng, X. M., Fan, H. T, Pan, S. S., Ye, C. and G. H. Lia, 2006, Optical properties of amorphous GaAs1-xNx film sputtering with different N2 partial pressures, J. Vac. Sci. Technol. A 24 : 1714.

- Vedam K., Mcmarr P.J.and Narayan J., 1985, Nondestructive depth  profiling by spectroscopic ellipsometry, Appt. Phys. 47:339.