A Novel Design of Active Imidazolylquinoline Thin Film Organic Device Antenna

Shen Cherng1, Anchi Yeh2, Hsien-Chiao Teng3

1Department of Electrical Engineering, Chengshiu University, Niaosong, Kaohsiung, Taiwan, ROC 833

2Department of Chemical and Material Engineering and, Chengshiu University, Niaosong, Kaohsiung, Taiwan, ROC 833, scteng@mail.cma.edu.tw

3Department of Electrical Engineering, ROC Military Academy, Fengshan, Kaohsiung, Taiwan, ROC 830

Abstract: A novel design of the active NIQ/Cu thin film organic device antenna is demonstrated. The purpose of this antenna is applicable to study the promotion of the mobility of the electrons in organic device. [The Journal Of American Science. 2007;3(4):93-96]. (ISSN: 1545-1003).

Key words: organic active device; mobility; imidazolylquinoline; antenna

- Introduction

Recently, many designs of characterized organic devices including all types of organic light emission diode (OLED), organic thin film transistor (OTFT) have been reported [1, 2]. Modifying the organic complex and substrate can manoeuvre the characteristics of the device. Applying the technique of the fabrication of the planar organic device and the field measurement of the microstrip patch antenna, NIQ/Cu thin film component on the FR4 substrate can be function as a patch antenna with active organic device (OD) to express special characteristic of the device. Based on the shifting of the operation frequency of the active NIQ/Cu OD antenna in comparison with the micropstrip patch antenna resonated at TM11 mode, the dielectric coefficient and the carrier mobility of the carriers in device can be revealed by basic analysis. A simple geometry thin film active NIQ/Cu OD antenna was designed for the S-band at 2.4GHz and presented in this letter. Setting a truncated NIQ/Cu thin film patch OD at 1000/2000 nm (NIQ/Cu) in thickness is for the consideration of circular polarized field transmitted from the patch of NIQ/Cu, which may promote the mobility of the hop electrons at a specific direction provided by NIQ thin film as well as the conduction electrons from the copper [3].

II. Design of the device

An architectural schematic drawing of the truncated 2000 nm thick rectangular cooper patch with depositing 1000nm dielectric organic thin film NIQ is depicted in Figure 1 where the probe-feeding is at distance of 5.1mm to the centre of the patch. Meanwhile, the thickness of the substrate is 1.6mm. SMA connector with characteristic impedance Zo (50 Ω), loss tangent ( tangentδ) and specific (r (4.4) for inexpensive FR4 substrate shown in the figure are regarded as major parameters in transmission line model (the size of ground is assumed infinite).

Refer to the reference [3], the mobility of the electrons and the loss tangent of the patch NIQ/Cu OD were calculated and listed in Table 2.

Table 1. Design parameters of the NIQ/Cu patch OD

(a) top and front view

(b) side view

Figure 1. Schematic geometry drawing of the active NIQ/Cu OD antenna

Figure 2. Field measurements of the proposed OD antenna with NIQ/Cu patch on FR4 substrate at thickness of 1.6mm

Figure 3.  Measurement of the Return Loss of the OD antenna (a) only with patch of cooper (b) with the NIQ (c) with the NIQ/Cu.

Table 2. Results of the Calculation

Figure 4.  Measurement of the Gain of the OD antenna. (a) only with patch of cooper (b) with the NIQ

(c) with the patch of  NIQ/Cu.

Figure 4 depicts the measurement of the radiation gain of the active NIQ/Cu OD antenna [4].

- Calculation Results and Conclusion

An active electronic material, 2-(naphtho[3,4]imidazol-2-yl) quinoline (NIQ), 1, has been synthesized and fully characterized [5]. This compound exhibits field-effect carrier mobility and behaves as a p-type semiconductor (mobility coefficient μ = 0.148×10-4 m2/Vs at VDS = 10 V). NIQ and its related imidazolylquinoline compounds may have possible applications as active materials in organic thin film active OD antenna.The calculation has shown the loss tangent of NIQ is 10-4 and the dielectric coefficient is 0.94 for the NIQ thin film. Those values are patch OD thickness related. In contrast, as we know hop electrons affect the displacement current in OD, since displacement and the conduction current is up to 10+8 for the NIQ/Cu active OD antenna, the conduction current is dominated and shall be regarded as the major parameter controlling the characteristics of the OD. Moreover, for the radiation efficiency (gain) is highly related to the loss tangent and the dielectric coefficient, the organic active device can be used as the modulator of the microstrip antenna.

Correspondence to:

Hsien-Chiao Teng

Assistant Professor

Department of Electrical Engineering

ROC Military Academy

scteng@mail.cma.edu.tw

Telephone: 88677479510

References

- (a) Horowitz, G.;Hajlaoui, R.;Bourguiga, R.;Hajlaoui, M. Synth. Met. 1999, 101, 401; (b) Guillaud, G.; Chaabane, B. R.;Jouve, C.;Gamoudi, M. Thin Solid Films 1995, 258, 279; (c) Lin, Y.-Y.;Gundlach, D. J.;Nelson, S. F.;Jackson, T. N. IEEE Trans. Electron Dev. 1997, 44, 1325.

- Alexandre Vial and Thierry Laroche ”Description of dispersion properties of metals by means of the critical pointsmodel and application to the study of resonant structures using the FDTD method” J. Phys. D: Appl. Phys. 40 (2007) 7152–7158

- Pankaj Kumar, S C Jain, Vikram Kumar, Suresh Chand, M N Kamalasanan and R P Tandon “Study of electron mobility in small molecular SAlq by transient electroluminescence method” J. Phys. D: Appl. Phys. 40 (2007) 7313–7317

- KL Wong, Planar antennas for wireless communications, Chapter 5~7, John Wiley & Sons, New York, NY.2003

- Tsun-Ren Chen,Anchi Yehb and Jhy-Der Chen ”A new imidazolylquinoline for organic thin film transistor”, Tetrahedron Letters 46 (2005) 1569–1571