Extrudate versus Powder Silica Alumina as Support for Re2O7 Catalyst in the Metathesis of Seed Oil-Derivatives – A Comparison

Bassie B. Marvey

Department of Chemistry, North-West University P/Bag X2046 Mafikeng, South Africa; Tel. +27-18-389-2527; Fax: +27-18-389-2052; E-Mail: bassie.marvey@nwu.ac.za

Abstract: Self- and cross-metathesis of fatty acid methyl esters (FAMEs) was investigated using silica alumina supported Re2O7 catalyst. Although a 3wt% Re2O7/SiO2-Al2O3/SnBu4 is already active for the metathesis of unsaturated FAMEs, the results have shown that particle size of silica alumina support has a profound influence on its activity and selectivity. Consequently high substrate conversions coupled with improved product yields (for mono- and diesters) and reaction rates were obtained upon using powder as opposed to extrudate silica alumina as the support material. Diesters are platform compounds for the synthesis of polymers and fragrances. In this paper a comparative outline of the influence of particle size of silica alumina (extrudate versus powder) on catalytic performance of a 3wt% Re2O7/SiO2-Al2O3/SnBu4 for self- and cross-metathesis of FAMEs is made. Low surface area and diffusion constraints associated with extrudates have been identified as some of the factors leading to low catalytic activity and selectivity.

Keywords: Olefin metathesis, extrudate silica alumina, powder silica alumina, 3wt% Re2O7/SiO2-Al2O3/SnBu4

Introduction

The first report on the heterogeneously catalysed metathesis of unsaturated esters was the work by Verkuijlen et al. [1] using Re2O7 supported on γ-Al2O3. Later on other support materials were found to be also effective including silica alumina (SiO2­Al2O3) with varying Al2O3 content [2-5]. The use of SiO2­Al2O3 support on Re2O7 catalyst resulted in improved catalytic performance compared to γ-Al2O3 [2]. Furthermore, a SiO2­Al2O3 support with 24.3% Al2O3 content was the most active of all other SiO2­Al2O3 types used [2]. Hence for this study SiO2­Al2O3 with 24.3% Al2O3 was the support of choice. Silica alumina is characterized by Brönsted acidity which accounts for its pronounced activity.

The metathesis of unsaturated fatty acid methyl esters (FAMEs) is an elegant method for the single-step synthesis of n-olefins, mono- and diesters of varying chainlengths and unsaturation [6-8]. Such products could find application as platform chemicals for the synthesis of niche market products. Monounsaturated fatty esters can, for example, be converted via a self-metathesis reaction into unsaturated diesters which are interesting starting materials for the synthesis of cross-linked unsaturated polyesters and polyamides [7]. Through cross metathesis with short-chain alkenes, long-chain fatty esters can be shortened into detergent-range C12-C14 acid esters [9]. Cross-metathesis of methyl oleate with 3-hexene, for example, gives 3-dodecene and methyl 9-dodecenoate as illustrated in Scheme 1 [9]:

Scheme 1. Cross-metathesis of methyl oleate with 3-hexene.

The abundance of unsaturated fatty acids and esters in animal fats and plant oils presents us with the opportunity to exploit these materials as renewable alternatives to petroleum-based feedstocks [10-14]. Direct transformation of unsaturated fats and oils by metathesis results in the formation of detergent-range alkenes and high molecular weight macromolecules with improved drying properties [7, 15]. Hence the metathesis of fatty oils provides a novel way of producing feedstocks from a readily available and cheap raw material.

The main challenge, however, is to find highly active, selective and stable catalysts that can withstand deactivation under a broad range of organic functional groups.  Previously we reported the self- and cross-metathesis of sunflower oil-derived fatty esters using powder 3wt% Re2O7/SiO2-Al2O3 catalyst [16]. In this paper a comparative outline of the influence of particle size of silica alumina (extrudate versus powder) on the activity and selectivity of a 3wt% Re2O7/SiO2-Al2O3/SnBu4 for self- and cross-metathesis of FAMEs is presented. Previous related work by other authors focused primarily on the variation of alumina content in silica alumina in a single component subtrate system, namely, methyl oleate [2, 5]

Materials and Methods

Hexanes (Aldrich) were dried by refluxing over sodium and were subsequently stored under an argon atmosphere. Methyl linoleate (99%, Aldrich), methyl oleate (Aldrich, 99.0%) biodiesel and sunflower oil (Excella) were purified from peroxides by treatment with calcined SiO2-Al2O3 (24.3% Al2O3, AKZO) under N2 atmosphere. Silica alumina was purchased in extrudate form from which powder silica alumina (120-180 μm particle diameter) was prepared.  Biodiesel was prepared from sunflower oil by transesterification using methanol [5, 8]. Ammonium perrhenate (NH4ReO4, FLUKA or STREM) and tetrabutyl tin (SnBu4, 93%, Aldrich) were used as purchased. A 3wt% Re2O7/SiO2-Al2O3 catalyst was prepared by pore volume impregnation of SiO2-Al2O3 (0.97 g) with an aqueous solution of NH4ReO4 (0.0332g). The catalyst was dried at 120 °C followed by calcination in air at 550 °C for 3 h and subsequently under N2 for 1 h. To 0.2g of 3wt% Re2O7/SiO2-Al2O3 catalyst in a glass reactor, 2 mL of solvent (hexanes) and 5 μL of the SnBu4 were added in that order followed by 0.5 mL of the substrate after 2 min. of stirring. Samples were collected at regular time intervals with a syringe and were analysed by FID-GC equipped with a DB-1 fused silica capillary column and GC/MS as previously described [16].

Results and Discussion

Self-metathesis of methyl linoleate

Self-metathesis of methyl linoleate resulted in a mixture of n-olefins, monoesters and diesters (Scheme 2). Figure 1 shows a typical gas chromatogram for the products resulting from self-metathesis of methyl linoleate as well as its cross-metathesis with methyl oleate. Table 1 presents total metathesis and the yields for n-olefins, monoesters and diesters obtained with extrudate and powder silica alumina as support materials for a 3wt% Re2O7 catalyst. Total metathesis represents the sum of all product yields in mol% and serves as an indicator for metathesis activity. Upon using powder silica alumina, a total metathesis of 86.1% was obtained compared to 68.6% with extrudate silica alumina support. The yields obtained with powder silica alumina for n-olefins, monoesters and diesters were 28.1, 37.5 and 20.4%, compared to extrudate silica alumina with 28.5, 24.1 and 16% for n-olefins, monoesters and diesters, in that order. The use of powder silica alumina brought an improvement in mono- and diester yields by 35.7 and 21.6%, respectively. On the other hand, a slight decrease in n-olefins by 1.4% was obtained.

The relatively low activity by extrudate 3wt% Re2O7/SiO2-Al2O3 catalyst could be attributed to low surface area and diffusion constraints which have a negative bearing on catalyst-substrate contact, resulting consequently to lower product yields and reduced reaction rates. A slight improvement in catalytic activity was, however, observed when extrudate silica alumina support was first pretreated by impregnating it with an aqueous solution of either 2wt% PO43- or 2wt% Cs+ ions. Pretreatment with 2wt% PO43- or 2wt% Cs+ ions led to an improved substrate conversion by 3.3 and 7.6%, respectively. These results were in agreement with those previously reported by du Plessis and coworkers for 1-octene [17]. However, Mol and Andreini [18] observed only an improvement in selectivity upon treatment of silica alumina with 2wt% Cs+ ions in 1-octene metathesis.

Cross-metathesis of methyl linoleate with methyl oleate

Cross-metathesis of methyl oleate and methyl linoleate resulted in a mixture of n-olefins, monoesters and diesters. Table 2 presents the total metathesis and the yields obtained with extrudate and powder silica alumina as support materials. Total metathesis of 66.8% was obtained in the presence of extrudate silica alumina after 5 h, which represents a decrease in activity by 2.6% compared to self metathesis of methyl linoleate using the same type of silica alumina. On the other hand, total metathesis of 76.2% was attained in 3 h with powder silica alumina support, an improvement in activity by 14.1% relative to extrudate silica alumina supported catalyst. The yields obtained with powder silica alumina for n-olefins, monoesters and diesters were 23.4, 33.4 and 19.4% compared to extrudate silica alumina with 38.0, 22.8 and 6.0% for n-olefins, monoesters and diesters, in that order. This represents an improvement in mono- and diester yields by 46.5 and 223.3%, respectively. On the other hand, a decrease in n-olefins by 38.4% was observed. Furthemore, higher molecular weight olefins (( C21), monoesters (( C25) and diesters (( C26) were not observed upon using extrudate 3wt% Re2O7/SiO2-Al2O3/SnBu4 catalyst, probably as a result of a relatively low substrate conversion. These products were, however, observed with a powdered support.

Scheme 2. Self-metathesis of methyl linoleate.

In spite of the differences in catalytic activity, both powder and extrudate silica alumina supported Re2O7 catalysts showed preferential selectivity for products with fewer carbon-carbon double bonds. For that reason selectivity decreased in the order: monoenes > dienes > tetraenes > trienes > tetraenes. It follows, therefore, that higher yields obtained were for the compounds containing fewer carbon-carbon double bonds than was the other way round.

Table 1 Yields of products resulting from self-metathesis of methyl linoleate using a 3% Re2O7/SiO2-Al2O3/SnBu4 catalytic system (Substrate (0.5 mL), catalyst (0.2g), temp (20 °C))

| Type of SiO2-Al2O3 | Yield/% |
| --- | --- |
|  | n-Olefins | Monoesters | Diesters | Total metathesis | Time/h |
| Extrudates | 28.5 | 24.1 | 16.0 | 68.6 | 4 |
| Powder | 28.1 | 37.5 | 20.4 | 86.1 | 2 |

Table 2. Yields of products resulting from cross-metathesis of methyl oleate (MO) with methyl linoleate (ML) using a 3wt% Re2O7/SiO2-Al2O3/SnBu4 catalytic system

| Type of SiO2-Al2O3 | Yield/% |
| --- | --- |
|  | n-Olefins | Monoesters | Diesters | Total metathesis | Time/h |
| Extrudates | 38.0 | 22.8 | 6.0 | 66.8 | 5 |
| Powder | 23.4 | 33.4 | 19.4 | 76.2 | 3 |

ML/MO molar ratio = 3/1; Substrate (0.5 mL), catalyst (0.2g), temp (20 °C)]

Metathesis of FAMEs derived from sunflower oil

Whereas previously we reported the metathesis of FAMEs from sunflower oil using a powdered 3wt% Re2O7/SiO2-Al2O3/SnBu4 catalytic system [16], we now report the metathesis of the same using extrudate silica alumina supported 3wt% Re2O7/SiO2-Al2O3/SnBu4 catalyst. The substrate mixture was composed of palmitate (7.3%), stereate (6%), oleate (20.6%), linoleate (65.1%), arachidate (0.3%), and behenate (0.7%). Table 3 compares the total metathesis and the yields obtained with extrudate and powder silica alumina supports. After 3 h reaction time, the total metathesis was 72.2% with powder silica alumina supported Re2O7 catalyst compared to 66.7% after 5 h with extrudate silica alumina support. These values represent an improvement in activity by 8.2% when powder silica alumina support is employed instead of extrudate silica alumina. The product yields obtained using the latter were 32.5, 25.2 and 9.4% after 5 h for n-olefins, monoesters and diesters compared to 26.0, 27.8 and 18.4% after 3 h, in that order, with a powdered support. Clearly there was an improvement in mono- and diester yields by 10.3 and 95.7%, respectively. On the other hand, the yield for n-olefins decreased by 20%. Indeed the results obtained and the trends observed show a strong agreement and demonstrate a profound influence of particle size of the support on the activity and selectivity of the Re2O7 catalyst.

Table 3. Yields of products resulting from metathesis of FAMEs (derived from sunflower oil) using a 3wt% Re2O7/SiO2-Al2O3/SnBu4 catalytic system (Substrate (0.5 mL), catalyst (0.2g), temp (20 °C))

| Type of SiO2-Al2O3 | Yield/% |
| --- | --- |
|  | n-Olefins | Monoesters | Diesters | Total metathesis | Time/h |
| Extrudates | 32.5 | 25.2 | 9.4 | 66.7 | 5 |
| Powder | 26.0 | 27.8 | 18.4 | 72.2 | 3 |

Conclusions

Although a 3wt% Re2O7/SiO2-Al2O3/SnBu4 is already active for the metathesis of unsaturated FAMEs, the results have shown that particle size of silica alumina support has a profound influence on its activity and selectivity. Relatively low substrate conversions and lower yields in mono- and diesters are obtained upon the use of extrudate silica alumina as the support material. On the contrary, higher conversions with improved product yields and reaction rates are obtained with powder silica alumina. Pretreatment of extrudate silica alumina with either 2wt% PO43- or 2wt% Cs+ ions could, however, bring about a slight improvement in its catalytic activity. The low surface area of extrudates together with diffusion constraints have been identified as some of the factors that account for the poor catalytic performance. Such constraints are minimal on silica alumina in powder form as a result of the high surface area of the support and the relatively easy contact between the substrate molecules and the catalytic active sites.

Acknowledgement

The National Research Foundation of South Africa (NRF) for financial support.

References and Notes

- Verkuijlen, E.; Kaptein, F.; Mol, J.C.; Boelhouwer, C. 1977. Heterogeneous metathesis of unsaturated fatty acid esters. J. Chem. Soc. Chem. Commun., 198-199.

- Xiaoding, X.; Mol, J.C. 1985. Re2O7/SiO2·Al2O3­SnR4 or PbR4, a highly active catalyst for the metathesis of functionalized alkenes. J. Chem. Soc., Chem. Commun., 631-633.

- Xiaoding, X.; Mol, J.C; Boelhouwer, C. 1986. Surface acidity of some Re2O7-containing metathesis catalyst. J. Chem. Soc., Faraday Trans. 82: 2707-2718.

- Xiaoding, X.; Boelhouwer, C; Vonk, D.; Benecke, J.I.; Mol, J.C. 1986. A model for the generation of active sites of rhenium-containing metathesis catalysts. J. Mol. Catal. 36: 47-66.

- Sibeijn, M.; Mol, J.C. 1991. Activity of supported Re2O7 catalysts for the metathesis of methyl oleate. Appl. Catal. 67: 279-295.

- Mol, J.C. 1983. Metathesis of functionalized olefins. Chemtech, 250-255.

- Van Dam, P.B.; Mittelmeijer, M.C.; Boelhouwer, C. 1974. Homogeneous catalytic metathesis of unsaturated fatty esters: New synthetic method for preparation of unsaturated mono- and dicarboxylic acids. J. Am. Oil Chem. Soc. 51: 389-392.

- Boelhouwer, C.; Mol, J.C. 1984. Metathesis of fatty acid esters. J. Am. Oil Chem. Soc. 61: 425-430.

- Mol, J.C. 2002. Applications of olefin metathesis in oleochemistry: an example of green chemistry. Green Chem. 4: 5-13.

- Marvey, B.B.; Segakweng, C.K.; Vosloo, H.C.M. 2008. Ruthenium carbene mediated metathesis of oleate-type fatty compounds. Int. J. Mol. Sci. 9: 615-625.

- Marvey, B.B. 2008. Sunflower-based feedstocks in nonfood applications: perspectives from olefin metathesis. Int. J. Mol. Sci. 9: 1393-1406

- Warwel, S.; Brüse, F.; Demes, C.; Kunz, M.; Rüsch gen. Klaas M. 2001. Polymers and surfactants on the basis of renewable resources. Chemosphere 43: 39-48

- Warwel, S.; Demes, C.; Steinke, G. 2001. Polyesters by lipase-catalyzed polycondensation of unsaturated and epoxidized lon-chain α,(-dicarboxylic acid methyl esters with diols. J. Polym. Sci., Part A: Polym. Chem. 39: 1601-1609

- Warwel, S.; Wiege, B.; Fehling, E.; Kunz, M. 2001. Copolymerization of ethylene with (-unsaturated fatty acid methyl esters using cationic palladium complex. Macromol. Chem. Phys. 202: 1114-1121.

- Thich, G.K.; Borene, M.; Edwards, E.; Tam, W-P. 1999. Metathesis of soybean oil, www.geocities.com/gthich/soybean.htm (accessed 12/09/08)

11/20/2008

- Marvey, B.B.; Du Plessis, J.A.K.; Vosloo, H.C.M.; Mol, J.C. 2003. Metathesis of unsaturated fatty acid esters derived from South African sunflower oil in the presence of a 3 wt% Re2O7/SiO2–Al2O3/SnBu4 catalyst. J. Mol. Catal. A: Chem. 201: 297-308.

- Du Plessis, J.A.K.; Spamer, A.; Vosloo, H.C.M. 1998. Re2O7/SiO2–Al2O3/SnMe4/1-octene catalytic system Part I: The influence of Cs+ and PO43- on the metathesis activity. J. Mol. Catal. A:Chem. 133: 175-180.

- Mol, J.C.; Andreini, A. 1998. Activity and selectivity of rhenium-based catalysts for alkene metathesis. J. Mol. Catal. 463: 151-156.

# Text boxes

Figure 1. Gas chromatogram of the metathesis products of methyl linoleate: n-olefins (peaks 1-3, 5, 7), monoesters (peaks 4, 6, 8, 10, 12) and diesters (peaks 9, 11, 13, 14)