Model for Predicting the Concentration of Sulphur Removed during Temperature Enhanced Oxidation of Iron Oxide Ore

C. I  Nwoye*a ,  S. U Ofoegbub ,  U. C Nwoyec ,  S. Inyamad  ,  H. Ekea  and C. Nlebedime

aDepartment of Materials and Metallurgical Engineering Federal University of Technology, Owerri, Nigeria.

bDepartment of Materials Science, Aveiro, University Portugal.

cData Processing, Modelling and Simulation Unit, Weatherford Nig. Ltd. Port-Harcourt Nigeria.

dDepartment of Industrial Mathematics, Federal University of Technology, Owerri, Nigeria

eDepartment of Materials Science, University of Cadiff Wales, United Kingdom.

chikeyn@yahoo.com

Abstract

Model for predicting the concentration of sulphur removed during temperature enhanced oxidation of iron oxide ore has been derived. The model ; %S   =    0.1011   was found to predict the concent-

LogT

ration of sulphur removed, very close to the corresponding %S values obtained from the actual experimental process. It was found that the model is dependent on the values of the treatment temperature used during the desulphurization process. The validity of the model is believed to be rooted in equation (3) where both sides of the equation are correspondingly almost equal. The positive or negative deviation of each of the model-predicted values of %S from those of the corresponding experimental values was found to be less than 37% which is quite within the range of acceptable deviation limit of experimental results, hence showing the validity and usefulness of the model for predictive analysis.

Keywords: Model, Prediction, Sulphur Removed, Temperature, Oxidation, Iron Oxide Ore,

1. Introduction

Agbaja iron ore deposit is the largest known Nigerian iron ore deposit estimated at 1250 metric tonnes of ore reserve. It consists of oolitic and pisolitic structures rich in iron oxides, in a matrix that is predominantly clay. The principal constituent mineral is goethite, with minor hematite, maghemite, siderite, quartz, kaolinite pyrite and an average of 0.09%S (Uwadiele1984). Investigations made by Bardenheuer and Geller (1934) indicated that the sulphur transfer from metal to slag or slag to gas during desulphurization involves oxygen transfer in the opposite direction. They posited that the mechanism of such desulphurization involves oxidation of sulphur resident in the metal or slag by oxygen from the slag through ionic exchange between the oxygen and sulphur, since the whole system is made up of liquid/molten condition during this process. They maintained that oxygen in the slag comes from CaO, which is one of the products of decomposition of CaCO3 deposited into the slag as a slag forming agent.

St Pierre and Chipman (1956), on studying gas-slag system during iron making discovered that at oxygen partial pressure below about 10-5 atm., sulphur dissolves in the melt as sulphide ions; at oxygen partial pressure higher than 10-3 atm., sulphur enters the melt as sulphate ions. In both cases, they stated that both the sulphide and sulphate ions leave the furnace through the slag. They therefore concluded that the mechanism of such desulphurization process is oxidation of sulphur by oxygen from the slag through ionic exchange between the two participating elements.

It was found by Turkdogan and Darken (1961) that at a temperature well below about 16000C, the pyrosulphate reaction also occurs. They found that this reaction was an enhancement to the desulphurization process actually taking place in the furnace. Also oxygen for this process was found to come from the slag, engaging sulphur in ionic exchange; being the mechanism of such process.

It was discovered that one of the most important factors influencing the desulphurization process during iron making is the state of oxidation of the bath (Pehlke et.al 1975) .

The aim of this work is to derive a model for predicting the concentration of sulphur removed during temperature enhanced oxidation of Agbaja (Nigerian) iron oxide ore

2. Model

The solid phase (ore) is assumed to be stationary, contains some unreduced iron remaining in the ore. It was found (Nwoye,2008) that oxygen gas from the decomposition of KClO3 attacked the ore in a gas-solid reaction, hence removing (through oxidation) the sulphur present in the ore in the form of SO2 .Equations (1) and (2) show this.

2KClO3 (s)             2KCl (s)   + 3O2 (g)          (1)

S(s) Heat   S(g) + O2 (g)             SO2 (g)             (2)

2.1 Model Formulation

Experimental data obtained from research work (Nwoye,2007) carried out at SynchroWell Research Laboratory, Enugu were used for this work.

Results of the experiment as presented in report ( Nwoye, 2007) and used for the model formulation are as shown in Table 1.

Computational analysis of the experimental data shown in Table 1, gave rise to Table 2 which indicate that;                                        [(T)γ%S] =  α/kn   (approximately)               (3)

kn [(T)γ%S]   = α                                     (4)

Taking logarithim of both sides

Log (kn[(T)γ%S])= Log α                         (5)

Logkn+Log [(T)γ%S])   =  Log α             (6)

Logkn+ γ %SLogT  =  Log α                 (7)

γ%SLogT=  Logα  -  Log kn                  (8)

%S   =   Logα  -  Logkn                   (9)

γ LogT

Introducing the values of α , kn and γ into equation (9) (since the are constants) and evaluating further, reduces it to;

%S   =          0.1011                              (10)

LogT

Therefore

%S   =                Df                                  (11)

LogT

Where                                                                                                                                                                                                            %S = Concentration of sulphur removed

during the pyrometallurgical-oxidation

process.

kn = 8.30 (Decomposition coefficient of

KClO3 relative to its weight input (10g

per 50g of the iron ore) determined in

the experiment (Nwoye,2007)

(γ)=  0.8 (Temperature coefficient relative

to weight-input of KClO3) determined

in the experiment (Nwoye,2007)

(α) = Weight of KClO3 added as oxidant (g)

T = Treatment temperature used for the

process (0C)

Df =0.1011 (Assumed desulphurization

enhancement factor)

Table 1: Variation of concentration of sulphur removed with treatment temperature (Nwoye,2007)

| T(0C) | Μ | %S |
| --- | --- | --- |
| 500 550 600 650 700 750 | 50 50 50 50 50 50 | 0.030 0.035 0.040 0.043 0.050 0.055 Table 1: Variation of concentration of dissolved iron with weight input of iron oxide ore and final solution pH. (Nwoye;2006) |

Table 2: Variation of α/kn with Tγ%S

| α/kn | Tγ%S |
| --- | --- |
| 1.2048 1.2048 1.2048 1.2048 1.2048 1.2048 | 1.1608 1.1932 1.2272 1.2496 1.2996 1.3381 |

3. Boundary and Initial Condition

Consider iron ore (in a furnace) mixed with potassium chlorate (oxidant). The furnace atmosphere is not contaminated i.e (free of unwanted gases and dusts). Initially, atmospheric levels of oxygen are assumed just before the decomposition of KClO3 (due to air in the furnace).Weight, M of iron oxide ore used; (50g), and treatment time; 360secs. were used. Treatment temperature range; 500-750oC, ore grain size; 150µm, and weight of KClO3 (oxidant); 10g were also used. These and other process conditions are as stated in the experimental technique (Nwoye; 2007).

The boundary conditions are: furnace oxygen atmosphere due to decomposition of KClO3 (since the furnace was air-tight closed) at the top and bottom of the ore particles interacting with the gas phase. At the bottom of the particles, a zero gradient for the gas scalar are assumed and also for the gas phase at the top of the particles. The reduced iron is stationary. The sides of the particles are taken to be symmetries.

4. Model Validation

The formulated model was validated by direct analysis and comparism of %S values predicted by the model and those obtained from the experiment for equality or near equality.

Analysis and comparism between these %S values reveal deviations of model-predicted %S values from those of the experiment. This is attributed to the fact that the surface properties of the ore and the physiochemical interactions between the ore and the oxidant (under the influence of the treatment temperature) which were found to have played vital roles during the oxidation process (Nwoye, 2007) were not considered during the model formulation. This necessitated the introduction of correction factor, to bring the model-predicted %S values to those of the experimental %S values (Table 3).

Deviation (Dv) (%) of model-predicted %S values from experimental %S values is given by

Dv =   Dp – DE   x  100 	              (12)

DE

Where     Dp = Predicted %S values from

model

DE  =  Experimental %S values

Correction factor (Cf ) is the negative of the deviation i.e

Cf     = -Dv                                          (13)

Therefore

Cf  = -    Dp – DE     x 100 	           (14)

DE

Introduction of the corresponding values of Cf from equation (14) into the model gives exactly the corresponding experimental %S values. (Nwoye, 2007)

5. Results and Discussion

The derived model is equation (10) or (11). A comparism of the values of %S from the experiment and those from the model shows minimum positive and negative deviations less than 37% which is quite within the acceptable deviation limit of experimental results hence depicting the reliability and validity of the model. This is shown in Table 3.

The validity of the model is believed to be rooted in equation (3) where both sides of the equation are correspondingly almost equal. Table 2 also agrees with equation (3) following the values α/kn and Tγ%S evaluated from Table 1 as a result of corresponding computational analysis.

The value 0.1011 has a direct relationship with the value of %S as shown in equation (10). This indicates that the constant contributes directly (as a multiplying factor) to the predicted concentration of sulphur removed from the ore. Based on the foregoing, the constant is denoted as desulphurization enhancement factor Df .

Table 3: Comparism between %S removed as predicted by model and as obtained from experiment. (Nwoye ,2007)

Where %Sexp = %S values from experiment

(Nwoye,2007)

%SM = %S values predicted by model

6. Conclusion

The model predicts the concentration of sulphur removed during temperature enhanced oxidation of Agbaja iron oxide ore. The validity of the model is believed to be rooted in equation (3) where both sides of the equation are correspondingly almost equal. The deviation of the model-predicted %S values from those of the experiment is less than 37% which is quite within the acceptable deviation limit of experimental results.

| %Sexp | %SM | Dv (%) | Cf (%) |
| --- | --- | --- | --- |
| 0.030 0.035 0.040 0.043 0.050 0.055 | 0.0375 0.0369 0.0364 0.0360 0.0355 0.0352 | +25.00 +5.43 -9.00 -16.28 -29.00 -36.00 | -25.00 -5.43 +9.00 +16.28 +29.00 +36.00 |

Further works should incorporate more process parameters into the model with the aim of reducing the deviations of the model-predicted %S values from those of the experiment

Acknowledgement

The authors thank Dr. Ekeme Udoh, a  modelling expert at Linkwell Modelling Centre Calabar for his technical inputs. The management of SynchroWell Nig. Ltd. Enugu is also appreciated for permitting and providing the experimental data used in this work.

References

Bardenheuer, P and Geller, W.,(1934) . Mitt.

Kais. Wilh. Inst., Eisenforsch., vol. 16, P77-

91.

Nwoye, C I ; (2007). SynchroWell Research

Work  Report, DFM Unit, No 2007146,

35-45.

Nwoye, C I ; (2008) . Process Analysis and

Mechanism of Desulphurization of Agbaja

Iron Oxide Ore. JMME vol. 8 27-32.

Pehlke, R.D., Porter,W.F.,Urban,R.F.,and Gaines,

J.M;(1975) . BOF, Steel Making, Iron &Steel

Soc. AIME vol 2. P142- 153.

St. Pierre, G.R and Chipman, J.,(1956).Trans.

AIME, vol. 206, P1474-83.

Turkdogan, E.T., and Darken, L.S.,(1961); Trans.

Met. Soc. AIME, vol. 221, P464-74.

Uwadiele, G .G.O.O., (1984). Beneficiation

Studies of Agbaja Iron Ore. Ph.D Thesis,

Univerity of Strathdyde, p341

1/27/2009