Models for Predicting the Hardness of the Heat Affected Zone in Mild Steel Weldments Cooled in Water, Air, Palm Oil, Kerosine and Groundnut Oil

C. I.  Nwoye*1, A. I. Ogbonna1, M. C. Obi2, J. E. O. Ovri1 and E. Nnuka3

1Department of Materials and Metallurgical Engineering, Federal University of Technology, P.M.B 1526, Owerri, Nigeria.

2Department of Industrial Mathematics, Federal University of Technology, P.M.B 1526, Owerri, Nigeria.

3Department of Materials and Metallurgical Engineering, Nnamdi Azikiwe University, P.M.B 5025, Awka, Nigeria.

chikeyn@yahoo.com

Abstract

Model for predicting the hardness of HAZ in mild steel weldment cooled in any of; groundnut oil,  kerosine, palm oil, air, and water has been derived. The model; 4γ = 0.92β + 0.92φ + 0.94θ + 0.84α predicted directly HAZ hardness values γ, β, φ, θ, and α. Their respective deviations from the corresponding experimental values were found to be less than 1.6% which is quite insignificant and within the acceptable range of deviation limit from experimental results. The coefficient associated with each HAZ hardness value (β, φ, θ, and α) was found to be the numerical equivalent of the microstructural resistance to the hardening of the HAZ during cooling and are generally expressed as Coefficient of Hardness or Hardenability Factor. These coefficients were found to have inverse relationship with the associated HAZ hardness values along the model equation.

Keywords: Model, Hardness, Heat Affected Zone, Mild Steel, Weldments.

1. Introduction

Arc welding may be defined as the process where by the heat generated by the electric arc is maintained in most cases between the electrodes and the work piece (Lancaster, 1993). The arc supplies enough heat to melt the base metal in the vicinity of the arc and also the electrode. In arc welding, some of the processes utilize consumable electrodes which serve to strike an arc onto the work pieces, and they melt to provide the weld metal. In recent times, advancements has been made in such joining processes as adhesives, mechanical fasteners, brazing

soldering (Callister, 1996). However, welding remains the most important metal joining process.  Several processes and methods of arc welding exist, for example carbon-arc welding, atomic hydrogen welding, shielded metal arc welding, plasma arc welding, electroslag welding, etc. (Davies, 1993; Higgins, 1994). Arc welding is the most widely used fusion welding process. It produces smooth welding surfaces and utilizes both direct and alternating current. Oxidation is minimal as weld metal is completely shielded from the atmosphere.        The process is excellent welding low carbon, medium carbon and alloy steels. The arc is quiet, discomfort from glare or fume is minimal, and is applicable in fabricating vessels, boilers and pipes, etc. Disadvantages of the process include need for very high current for welding operations and formation of a crater in the molten metal of the work piece arising from the pressure produced by the stream of ions flowing from the cathode (Higgins, 1994). Electrodes are the elements of an arc lamp or furnace between which an arc is struck. They are filler materials which a joining engineer should be able to match with the parent material to avoid failure (Davies, 1993). Uncoated electrodes produce an atmosphere of oxygen and nitrogen, so that the oxides and nitrides formed may be in the weld metal, thus impairing ductility and impact toughness in the weld. The situation is avoided by use of coated electrodes, which contains slag and so form a fluid covering over the weld (Higgins, 1994). In this case, stabilization of the arc is achieved by including materials which would produce ionization and consequently may be wielded by the metallic arc process. In welding carbon and low carbon steels, coated electrodes are used especially for low carbon steels but for alloy steels in which martensite occurrence is likely on cooling and formation of hydrogen embrittlement expected, the electrode coating must be free from hydrogen forming cellulose (Higgins, 1977).

Weldment cracking is one of the reasons for low mechanical properties such as hardness and impact strength in welded parts. Adjacent to the immediate welded area or fusion zone is the heat affected zone (Nnuka etal., 2008). The mechanical property of main importance in HAZ is the hardness since it gives an indication of the degree of embrittlement there. It was found (Lancaster, 1987) that the heat affected zone hardness produced by any given welding operation depends on the cooling rate experienced by the HAZ. Too rapid rate of cooling favours the formation of hard and brittle martensite in all the sub zones of the HAZ or increases the martensite region in size relative to the other regions. The presence of martensite in the HAZ results in a very high hardness value for the heat affected zone. Slow cooling favours a better microstructure needed for engineering applications. Also, the more rapid the quenching rate, the greater the HAZ hardness.

From available literature, much has been done on different joining processes and methods, but no emphasis has been placed on the derivation of models for prediction or evaluation of the hardness of the heat affected zone (HAZ) in weldments cooled in different media; evaluation of the hardness of HAZ cooled in a particular medium as a function of the hardness of HAZ from the same material but cooled in different media. Researches carried out on HAZ; its cooling and mechanical properties have not addressed the issue of predicting or evaluating the hardness of the HAZ of a material cooled in a particular medium by simple substitution of the value of the hardness of HAZ from the same material, but cooled in different media. The hardness of HAZ in aluminum, cast iron and mild steel cooled in kerosine was found to be exactly the same as the hardness value of the same materials cooled in groundnut oil (Nwoye, 2008). This implies that

HG = HK                                          (1)

Where

HG  = Hardness of HAZ cooled in

groundnut oil

HK  = Hardness of HAZ cooled kerosine

Nwoye (2008) reported that 8-10% less hardness than that from water occurs when kerosine or groundnut oil is used as quenchant for HAZ. He discovered that quenching the HAZ with kerosine or groundnut oil gives approximately 8-10.7% more hardness than that from quenching with air. He found that palm oil gave the lowest hardness and cooling rate on the HAZ.

The present study aims at deriving a model for predicting the hardness of the heat affected zone in mild steel weldment cooled in water, air, palm oil, kerosine and groundnut oil. This way, for example, the hardness of HAZ in mild steel weldment cooled in water can be predicted or evaluated as a function of the hardness value of the HAZ of same mild steel material but cooled in any other medium or media (air, palm oil, kerosine and groundnut oil).

Table 1: Effect of cooling media on the hardness of the HAZ in mild steel weldments

| Coolants | Mild Steel Hardness (VHN) |
| --- | --- |
| Air | 471 |
| Palm oil | 503 |
| Groundnut | 513 |
| Kerosine | 513 |
| Water | 560 |

2. Materials and methods

Mild steel was cut and welded using the shielded metal arc welding technique and the hardness of the HAZ (cooled in water, air palm oil, kerosine and groundnut oil maintained at room temperature) tested. The hardness of the HAZ is as presented in Table 1. The full details of the experimental procedures and equipment used are presented in the report (Nwoye, 2008).

3. Model formulation

Experimental data obtained from research work (Nwoye, 2008) carried out at Metallurgical and Materials Engineering Department of Federal University of Technology, Owerri were used for this work. Results of the experiment as presented in the report (Nwoye,2008) and used for the model formulation are as shown in Table 1. Computational analysis of the experimental data (Nwoye, 2008) shown in Table 1 resulted in Table 2.

Table 2: Ratio of hardness of HAZ from air cooling to hardness of HAZ from other media

| γ/β γ/φ γ/θ γ/α | 471/513 471/513 471/503 471/560 | 0.92 0.92 0.94 0.84 |
| --- | --- | --- |

Table 2 shows that the hardness of HAZ in mild steel weldment cooled in air is a function of the hardness of HAZ in same weldment cooled in any other medium or media. Therefore,

CASE 1: Hardness in air as a function of 1

coolant

γ   =  0.92β                                          (2)

γ   =  0.92φ                                          (3)

γ   =  0.94θ                                          (4)

γ   =  0.84α                                          (5)

CASE 2: Hardness in air as a function of 2 coolants

Adding both sides of eqn. (2) and (3)

2γ = 0.92β + 0.92φ                                  (6)

Adding both sides of eqn. (2) and (4)

2γ = 0.92β + 0.94θ                                  (7)

Adding both sides of eqn. (2) and (5)

2γ = 0.92β + 0.84α                                  (8)

Adding both sides of eqn. (3) and (4)

2γ = 0.92φ + 0.94θ                                 (9)

Adding both sides of eqn. (3) and (5)

2γ = 0.92φ + 0.84α                                (10)

Adding both sides of eqn. (4) and (5)

2γ = 0.94θ + 0.84α                                (11)

CASE 3: Hardness in air as a function of 3 coolants

Adding both sides of eqn. (2)-(4)

3γ = 0.92β + 0.92φ + 0.94θ                    (12)

Adding both sides of eqn. (2), (3) and (5)

3γ = 0.92β + 0.92φ + 0.84α                       (13)

Adding both sides of eqn. (3)-(5)

3γ = 0.92φ + 0.94θ + 0.84α                       (14)

Adding both sides of eqn. (2), (4) and (5)

3γ = 0.92β + 0.94θ + 0.84α                       (15)

CASE 4: Hardness in air as a function of 4 coolants

Adding both sides of eqns. (2)-(5)

4γ = 0.92β + 0.92φ + 0.94θ + 0.84α         (16)

Eqn. (16) is regarded as the general model since it is made up of all the coolants considered during the model formulation.

Substituting into eqns. (2)-(16) the respective experimental values of β, φ, θ, and α from Table 1, the corresponding values of γ where calculated and results presented in Tables 3-7.

Where

γ  =  Model-predicted hardness of HAZ in

mild steel weldment cooled in air (VHN)

β =  Hardness of HAZ in mild steel

weldment cooled in groundnut oil (VHN) φ =  Hardness of HAZ in mild steel weldment

cooled in kerosine (VHN)

θ =  Hardness of HAZ in mild steel weldment

cooled in palm oil (VHN)

α = Hardness of HAZ in mild steel weldment

cooled in water (VHN)

4. Boundary and initial conditions

The welding was carried out under atmospheric condition. After welding, weldments were also maintained under atmospheric condition. Welding current and voltage used are 180A and 220V respectively. SiO2-coated electrodes were used to avoid oxidation of weld spots. The coolants used were maintained at 250C (room temperature). Volume of coolants used; 1000cm3. No pressure was applied to the HAZ during or after the welding process. No force due to compression or tension was applied in any way to the HAZ during or after the welding process. The sides and shapes of the samples are symmetries.

5. Model validation

Models formulated were validated my direct analysis and comparison of the γ and γexp values obtained from model and experiment (Nwoye, 2008) respectively for equality or near equality. The model values γ were obtained by substituting into eqns. (2)-(16) the respective values of β, φ, θ, and α from Table 1.

Analysis and comparison between γ and γexp  values reveal deviations of model data from the experimental data. This is attributed to the non- consideration of the chemical properties of the coolant and the physiochemical interactions between the mild steel and the coolant which is believed to have played vital roles in modifying the microstructure of the HAZ during the coolant process. These deviations necessitated the introduction of correction factor to bring the model-predicted γ values to exactly that of the corresponding experimental values.

Deviation (Dv) of model γ values from the corresponding experimental values; γexp is given by

Dv  =   γ  - γexp     x  100                    (17)

γexp

where   γ  = Hardness values from model

γexp = Hardness values from experiment

Correction factor (Cf) is the negative of the deviation i.e.

Cf  = -Dv                                          (18)

Therefore

Cf  = -100   γ  - γexp                          (19)

γexp

Based on the foregoing, addition of the values of Cf to the model data gives exactly the corresponding experimental values.

6. Results and discussion

A comparison of the HAZ hardness values from experiment and those of the model show model values very much within the range of the experimental values. Results of this comparison are presented in Tables 3-7. Model values of γ evaluated from eqns. (2)-(16) and tabulated in Tables 3-7 show that all the equations are valid since all of them gave almost the same values of γ. Tables 3-7 indicate that the respective deviations of the model-predicted hardness values γ from those of the corresponding experimental values γexp

are all positive and less than 0.4% which is quite negligible and within the acceptable model deviation range from experimental results. The validity of the model could be deduced from Table 7 where the average HAZ hardness predicted by derived models as a function of 1, 2, 3 and 4 coolants respectively were all equal. This invariably translates into respective equal deviations from the corresponding experimental values of HAZ hardness. This shows that any of the models can be used since the respective model ((eqns.(2)-(16)) deviations from experimental values in terms of HAZ hardness are very negligible (less than 0.4%). However, the lowest magnitude of deviation was found to be associated with 2-coolant usage.

The values of β and φ ( in Table 8 for 1, 2, 3 and 4 coolant usages) were predicted using eqns. (2), (8),(15) and (16) respectively which represents 1 derived model from each CASE (1-4). Figs. 1 and 2 show that the lowest and highest magnitude of deviation of model-predicted β and φ values from the corresponding experimental values occurred as a function of 2-coolant and 4-coolant usage respectively.

Values of θ (in Table 8 for 1, 2, 3 and 4 coolant usages) were predicted eqns. (4), (11), (15) and (16) respectively. This also represents 1 derived model from each CASE (1-4). Fig. 3 indicates that the lowest and highest magnitude of deviation of model-predicted θ values from the corresponding experimental values occurred as a function of  2-coolant and 3-coolant usage respectively. Furthermore, the values of α (as in Table 8 for 1, 2, 3 and 4 coolant usage) were predicted using eqns. (5), (8), (15) and (16) respectively.

These eqns. represent 1 derived model from each CASE (1-4). It was found (as shown in Fig. 4) that the lowest and highest magnitude of deviation of model-predicted α values from the corresponding experimental values occurred as a function of 2-coolant and 4-coolant usage respectively.

This is a clear indication that the derived model in CASE 4 (eqn.(16)) can predict the hardness of HAZ in mild steel weldment cooled in water, palm oil, kerosine and groundnut oil. Here the HAZ hardness in a particular coolant is predicted as a function of HAZ hardness in 4 other coolants. This was also found to be the same for air cooling where the HAZ hardness in mild steel weldment cooled in air was predicted as a function of the HAZ hardness from the same material achieved by cooling in palm oil, groundnut oil, water and kerosine.

Based on the foregoing, it could be seen that the predicted value of HAZ hardness in mild steel weldment cooled in any of the coolants; (palm oil, groundnut oil, kerosene, air or water is more accurate when the value is evaluated as a function of HAZ hardness from just one (1) different coolant. However, for clarity, eqn. (16) is considered for its general and wide application since it is made up of all the coolants considered during the model formulation. Based on this, the HAZ hardness in mild steel weldment cooled in palm oil, groundnut oil, kerosine, air or water can be evaluated and predicted as a function of the HAZ hardness values obtained by cooling in any of the coolants or consortium of coolants. This can be done by reducing eqn. (16) to the particular coolant or consortium of coolant of interest, and then reducing also the coefficient of β, φ, θ, or α at the L.H.S (depending on the HAZ hardness acting as the dependent variable) to the value of the no. of coolants present in the abridged model as the case may be. This is so because eqns. (2)-(16) show that the coefficient of the HAZ hardness acting as the dependent variable is equal to the no. of coolant or coolants present in a particular derived model. For example, to evaluate the HAZ hardness of mild steel weldment cooled in air as a function of HAZ hardness from cooling in water and palm oil, eqn. (16) reduces to 2γ = 0.94θ + 0.84α which from derivation is eqn. (11). Here, the coefficient of γ which act as the dependent variable is 2 because there are only two (2) coolants present in the abridged model of eqn. (16). Eqns. (2)-(16) and Tables 3-8 show that the coefficients of the HAZ hardness values (independent variables); β, φ, θ, or α (at the R.H.S) decrease with increase in the values of β, φ, θ, or α and increase with decrease in the values of β, φ, θ, or α along each model. This clearly indicates that the coefficient associated with each HAZ hardness value (β, φ, θ, or α) is the numerical equivalent of the micro structural resistance to the hardening of the HAZ during cooling in the particular coolant. For instance Table 1 shows that cooling in water gave the highest HAZ hardness value. Table 2 and eqns. (2)-

(16) show that this value was obtained at the lowest coefficient of its HAZ hardness. This shows that the microstructure of the HAZ cooled in water mustered the least resistance to hardening during the cooling process. Therefore, for clarity, these coefficients are regarded as Coefficient of Hardness or Hardenability Factor.

Table 3: Comparison of the Hardness of HAZ in mild steel weldment cooled in air as obtained from experiment and hardness from derived model (as a function of HAZ hardness from 1 other different coolant)

| N | Models derived | γ | γexp | Dv (%) | Cf (%) |
| --- | --- | --- | --- | --- | --- |
| 1 1 1 1 | γ = 0.92β γ = 0.92φ γ = 0.94θ γ = 0.84α | 471.96 471.96 472.82 470.40 | 471 471 471 471 | +0.20 +0.20 +0.39 -0.13 | -0.20 -0.20 -0.39 +0.13 |

Table 4: Comparison of the Hardness of HAZ in mild steel weldment cooled in air as obtained from experiment and hardness from derived model (as a function of HAZ hardness from 2 other different coolants)

| N | Models derived | γ | γexp | Dv (%) | Cf (%) |
| --- | --- | --- | --- | --- | --- |
| 2 2 2 2 2 2 | 2γ = 0.92β + 0.92φ 2γ = 0.92β + 0.94θ 2γ = 0.92β + 0.84α 2γ = 0.92φ + 0.94θ 2γ = 0.92φ + 0.84α 2γ = 0.94θ + 0.84α | 471.96 472.39 471.18 472.39 471.18 471.61 | 471 471 471 471 471 471 824 | +0.20 +0.30 +0.04 +0.30 +0.04 +0.13 | -0.20 -0.30 -0.04 -0.30 -0.04 -0.13 |

Table 5: Comparison of the Hardness of HAZ in mild steel weldment cooled in air as obtained from experiment and hardness from derived model (as a function of HAZ hardness from 3 other different coolants)

| N | Models derived | γ | γexp | Dv (%) | Cf (%) |
| --- | --- | --- | --- | --- | --- |
| 3 3 3 3 | 3γ = 0.92β + 0.92φ + 0.94θ 3γ = 0.92β + 0.92φ + 0.84α 3γ = 0.92φ + 0.94θ + 0.84α 3γ = 0.92β + 0.94θ + 0.84α | 472.25 471.44 471.73 471.73 | 471 471 471 471 | +0.27 +0.09 +0.15 +0.15 | -0.27 -0.09 -0.15 -0.15 |

Table 6: Comparison of the Hardness of HAZ in mild steel weldment cooled in air as obtained from experiment and hardness from derived model (as a function of HAZ hardness from 4 other different coolants)

| N | Models derived | γ | γexp | Dv (%) | Cf (%) |
| --- | --- | --- | --- | --- | --- |
| 4 | 4γ = 0.92β + 0.92φ + 0.94θ + 0.84α | 471.79 | 471 | +0.17 | -0.17 |

Table 7: Comparison of average hardness of HAZ (in each of CASES 1-4) in mild steel weldment cooled in air as obtained from the experiment and derived model

| N | γ | γexp | Dv (%) | Cf (%) |
| --- | --- | --- | --- | --- |
| 1 2 3 4 | 471.79 471.79 471.79 471.79 | 471 471 471 471 | +0.17 +0.17 +0.17 +0.17 | -0.17 -0.17 -0.17 -0.17 |

Table 8: Variation of HAZ hardness in mild steel weldment cooled in groundnut oil, kerosine, palm oil and water (as obtained from derived model) with no. of coolants present in derived model

| N | βexp | β | φexp | φ | θexp | θexp | αexp | α |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 2 3 4 | 513 513 513 513 | 511.96 512.61 510.63 509.59 | 513 513 513 513 | 511.96 512.61 510.63 509.59 | 503 503 503 503 | 501.06 501.70 510.63 509.59 | 560 560 560 560 | 560.71 559.57 557.40 556.26 |

Where

N = No. of coolants constituting the

corresponding model

γexp = Hardness of HAZ in mild steel

weldment cooled in air (as obtained

from experiment) (VHN)

βexp=Hardness of HAZ in mild steel weldment

cooled in groundnut oil (as obtained

from experiment) (VHN)

φexp= Hardness of HAZ in mild steel

weldment cooled in kerosine (as

obtained from experiment) (VHN)

θexp=Hardness of HAZ in mild steel

weldment cooled in palm oil (as

obtained from experiment) (VHN)

αexp=Hardness of HAZ in mild steel weldment

cooled in water (as obtained from

experiment) (VHN)

Conclusion

The derived model (general model) predicts the HAZ hardness of mild steel weldment cooled in any of; groundnut oil, kerosine, palm oil, air and water as a function of HAZ hardness from the other different four (4) coolants. The deviations of the model-predicted HAZ hardness (γ, β, φ, θ, and α) from the corresponding experimental values were least for γ, β, φ, θ, and α when each HAZ hardness is calculated as a function of just one (1) other different coolant. The coefficient associated with each HAZ hardness value (β, φ, θ, and α) is the numerical equivalent of the microstructural resistance to the hardening of the HAZ during cooling the particular coolant. Acknowledgement

They authors thank the management of Federal University of Technology, Owerri for providing the equipment used for this work.

References

Callister, W.D., (Jnr.) (1996). Material

Science and Engineering. An introduction,

1st Edition, Sydney John Wiley & Sons

inc. p852.

Davies,A. C., (1993). The Science and

Practice of Welding, 10th Edition,

Cambridge University Press, p521.

Higgins, R. A., (1977). Engineering

Metallurgy Part II, 2nd Edition, London,

ELBS, p466.

Higgins, R. A., (1994). Engineering

Metallurgy, Arc Welding Processes, 2nd

Edition, Edward  Arnold Publishers,

London.p57.

Lancaster, J. F., (1987). Metallurgy of

Welding: The Mechanical Properties of the

Heat Affected Zone, 4th Edition, Allen and

University, London. p45.

Lancaster, J. F., (1993). Metallurgy of

Welding 5th Edition, London. Chapman and

Hall p389.

Nnuka, E. E., Ovat, F. A., and Oseni, M. I.,

(2008). Effect of Electrode Types on the

Mechanical Properties and Structure of

Welded Steel Joints. JMME Vol. 3, No. 1.

Nwoye, C. I. (2008). Comparative Studies of

the Cooling Ability of Hydrocarbon

Based Media and their Effects on the

Hardness of the Heat Affected Zone

(HAZ) inWeldments JMME Vol.3, No.1