Model for Computational Analysis of Quantity of Heat Absorbed by Hydrogen Peroxide Solution relative to Weight-Input of Iron Oxide Ore during Leaching.

aNwoye C.I and bNwakwuo C.C

aDepartment of Materials and Metallurgical Engineering Federal University of Technology, Owerri, Imo State.

bOxford University United Kingdom

chikeyn@yahoo.com

Abstract

Model for computational analysis of heat absorbed by hydrogen peroxide solution (relative to the weight of iron oxide ore added) has been derived. The values of the heat absorbed Q as predicted by the model were found to agree with those obtained from the experiment that the leaching process is endothermic in nature hence the positive values of Q and the absorbed heat. The deviations of the predicted Q values from the experimental values were found to be within the acceptable range.

Keywords: Model, Computational Analysis, Heat Absorbed, Hydrogen Peroxide, Iron Oxide Ore, Leaching.

1. Introduction

The use of hydrogen peroxide as the oxidizing agent for hydrometallurgical processes has been increasingly studied. McKibben [1] studied the kinetics of aqueous oxidation of pyrite by hydrogen peroxide at pH 1-4 and 293-313K.

The dissolution of iron ore has most often been investigated in the presence of oxygen at elevated temperatures and pressures [2-6].

The mixed potential model of leaching assumes that the charge transfer processes occurring at the mineral surface are those that control the rate of dissolution [6].

Chemical leaching of an iron oxide ore (using chemicals containing hydrogen) involves the attack on the ore by hydrogen ions which act as reducing agents. The main function of these ions is to reduce the oxide ore to metallic or near metallic state depending on the concentration and nature of the chemical involved. When this happens, the hydrogen ions become oxidized to water. During this process, some iron and other components of iron dissolve in the solution.

The aim of this work is to derive a model for computational analysis of the heat absorbed relative to the weight-input of Itakpe (Nigerian) iron oxide ore during leaching using hydrogen peroxide (H2O2) solution.

2. Model

The solid phase (ore) is assumed to be stationary, contains the un-leached iron remaining in the ore. Hydrogen ions from the hydrogen peroxide attack the ore within the liquid phase in the presence of oxygen.

2.1 Model Formulation

Experimental data obtained form research work [7] carried out at SynchroWell Research Laboratory, Enugu were used for this work.

Results of the experiment as presented in report [7] and shown in Table 1 indicate that;

In Q  =  N (W)1/2   (approximately)           (1)

Therefore

Q  =  eN(√W)

(2)

Introducing the value of N into equation (2)

Q  =  e1.04(√W)	                                 (3)

where

Q= Quantity of heat energy absorbed by

hydrogen peroxide solution during the

leaching process (J)

N=  1.04(Weight-input coefficient)

determined in the experiment.[7]

W = Weight of iron oxide ore used (g)

Equation (3) is the derived model.

Table1: Variation of quantity of heat absorbed by H2O2 solution with weight of

iron oxide ore used.

| W (g) | N(√W) | Q (J) | InQ |
| --- | --- | --- | --- |
| 18 20 22 26 28 30 | 4.4123 4.6510 4.8780 5.3030 5.5032 5.6963 | 121.68 148.20 171.60 182.52 208.32 226.20 | 4.8014 4.9986 5.1452 5.2069 5.3391 5.4214 |

3. Boundary and Initial Condition

Consider iron ore in cylindrical flask 30cm high containing leaching solution of hydrogen peroxide. The leaching solution is stationary i.e (non-flowing). The flask is assumed to be initially free of attach bacteria. Initially, atmospheric levels of oxygen are assumed. Varying weights (18-30g) of iron oxide ore were used as outlined in Table 1. The initial pH of leaching solution; 7.34 and leaching time; 30 minutes were used. A constant leaching temperature of 25oC was used. Ore grain size; 150µm, volume of leaching solution; 0.1 litre and hydrogen peroxide concentration;0.28mol/litre were used.. These and other process conditions are as stated in the experimental technique [7].

The boundary conditions are: atmospheric levels of oxygen (since the cylinder was open at the top) at the top and bottom of the ore particles in the liquid and gas phases respectively. At the bottom of the particles, a zero gradient for the liquid scalar are assumed and also for the gas phase at the top of the particles. The leaching solution is stationary. The sides of the particles are taken to be symmetries.

4. Model Validation

The formulated model was validated by direct analysis and comparism of Q values from model data and those from the experimental data for equality or near equality.

Analysis and comparism between these data reveal deviations of model data from experimental data. This is believed to be due to the fact that the surface properties of the ore and the physiochemical interactions between the ore and leaching solution which played vital roles during leaching process [7] were not considered during the model formulation. This necessitated the introduction of correction factor, to bring the model data to that of the experimental values. (See Table 2)

Deviation (Dv) of model Q values from experimental Q values is given by

Dv =   Dp – DE  x  100 	(4)

DE

Where     Dp = Predicted data from model

DE  = Experimental data

Correction factor (Cf) is the negative of the deviation i.e

Cf  =  -Dv 			(5)

Therefore

Cf  =  -100   Dp – DE		(6)

DE

Introduction of the corresponding values of Cf from equation (6) into the model  gives exactly the corresponding experimental Q values. [7]

5. Results and Discussion

The derived model is equation (3). A comparism of the values of Q from the  experimental data and those from the model shows a maximum negative deviation of 32.23% and a maximum positive deviation  of 31.64%. This is shown in Table 2.

This is believed to be within a considerable experimental result variation range.

Table 2: Comparism between quantity of heat absorbed as predicted by model and as obtained from experiment.

| Qexp (J) | QM (J) | Dv (%) | Cf (%) |
| --- | --- | --- | --- |
| 121.68 148.20 171.60 182.52 208.32 226.20 | 82.46 104.69 131.37 200.93 245.47 297.77 | -32.23 -29.36 -23.44 +10.09 +17.83 +31.64 | +32.23 +29.36 +23.44 -10.09 -17.83 -31.64 |

where 	Qexp =  Q values from experiment [7]

QM   = Q values predicted by model.

Qexp and QM show that the leaching process is endothermic in nature, hence the positive values of Q and heat absorbed during the process.

6. Conclusion

The model was used to evaluate the quantity of heat absorbed by the leaching solution of H2O2 during leaching of Itakpe iron oxide ore. It was observed from Q values predicted by the model and those obtained from experiment [7] that leaching of the iron oxide ore using H2O2 is an endothermic process, hence the positive values of Q from both model and experiment indicating absorbed heat. Further works should incorporate more process parameters into the model with the aim of reducing the deviations of the model data from that of the experimental.

Acknowledgement

The author thanks Dr. Ekeme Udoh, a modelling expert at Linkwell Modelling Centre Calabar for his technical inputs. He also acknowledges the management of SynchroWell Nig. Ltd. Enugu for permitting and providing the experimental data used in this work.

References

[1] McKibben, M.A., Ph.D Thesis,Pennsylvania State University (1984)

[2] Bailey,L.K and Peter,E., Can. Metall. Q.,15 (1976): 333-344.

[3] Gerlach,J., Hahne,H andPawlek, F., Erzmetall, 19 (1966): 66-74.

[4] McKay,D.R andHalpern,J., Trans Metall. Soc. AIME, 6 (1958): 301-309.

[5] Vracar, R., Zh. Prikl.Khim., 60 (1987): 1458-

1465.

[6] Papangelakis,V.G  and Demopoulos, G.P.,

Hydrometallurgy, 26 (1991): 309-325.

[7] Nwoye, C I ; SynchroWell Research Work

Report, DFM Unit, No 2021176, 2007,

36 – 76.