The effects of nanophase SiO2 particles on the strength and workability of binary blended concrete

Corresponding Author: Alireza Naji Givi, a Institute of Advanced Technology, Universiti Putra Malaysia, 43400 UPM Serdang, Selangor, Malaysia.

E-mail: presidentship2022@yahoo.com , Phone: +60 176649192, Fax: +98-2122424990

Suraya Abdul Rashid, b Department of Chemical and Environmental Engineering, Faculty of Engineering, Universiti Putra Malaysia, 43300 UPM Serdang, Selangor, Malaysia. E-mail: suraya@eng.upm.edu.my, phone: +603-89466285; Fax: +603-86567120.

Farah Nora A. Aziz,  c Department of Civil Engineering, Faculty of Engineering, Universiti Putra Malaysia, 43300 UPM Serdang, Selangor, Malaysia. E-mail: farah@eng.upm.edu.my, phone: +603-89464406.

Mohamad Amran Mohd Salleh, d Department of Chemical and Environmental Engineering, Faculty of Engineering, Universiti Putra Malaysia, 43300 UPM Serdang, Selangor, Malaysia. E-mail: asalleh@eng.upm.edu.my , phone: +603-89466286; Fax: +603-86567120.

e Department of Technical and Engineering Sciences, Islamic Azad University (Saveh Branch), Felestin Sq., Saveh, Iran. E-mail: alinazari84@aut.ac.ir, phone: +98 255 2241511, Fax: + +98-2122424990.

Abstract

The purpose of this study is to develop the compressive strength and workability of concrete by partial replacement of cement with nanophase SiO2 particles. SiO2 nano-particles with the average diameter about 15 nm were used with four different contents of 0.5%, 0.1%, 1.5% and 2.0% by weight. The results showed that the use of nano-SiO2 particles up to maximum 1.5% replacement level produces concrete with improved strength. However, the ultimate strength of concrete was gained at 1.0% of cement replacement. The workability of fresh concrete was decreased by increasing the content of SiO2 nano-particles. It is concluded that partial replacement of cement with nanophase SiO2 particles improves the compressive strength of concrete and decreases its workability.

Key words: Nanophase SiO2 particles; compressive strength, workability.

1. Introduction

Over the last 15 years Ultra High Performance Concretes (UHPC) have become a vanguard  product in industrial and structural applications thanks to outstanding properties, such as compressive strength of 150–200 MPa, tensile strength of 8–15 MPa with significant remaining post-cracking bearing capacity, and remarkable fracture energy of 20–30 kJ/m2 [1].

Health monitoring of structures by embedded or attached sensors has been gaining increasing interest and is more effective to guarantee structural safety in service. However, smart concrete, which can sense its own strain and damage, is more attractive due to its strong mechanical properties and self-monitoring characteristics. Smart concrete with short carbon fiber has been systematically developed [2,3]. The advantages of intrinsically smart concrete in contrast to smart sensing materials such as optical fibers, piezoelectric sensors, etc. are low cost, great durability, absence of mechanical property degradation due to the embedding of sensors, etc. [2].

Recently, the effect of micro-SiO2 particles by adding rice husk ash to blended concrete has been reviewed by Naji Givi et al. [4]. Several researchers have demonstrated that the finer the SiO2 particle sizes in micron level, the higher the compressive strength. But there is a lack on nano-size particle’s effects. In this work, the effects of nano-SiO2 particles on compressive strength and workability of the blended concrete has been studied.

2. Materials and Methods

2.1. Materials and mixtures

2.1.1. Cement

Ordinary Portland Cement (OPC) obtained from Holcim Cement Manufacturing Company of Malaysia conforming to ASTM C150 standard was used as received. The chemical and physical properties of the cement are shown in Table 1.

2.1.2. Nano-SiO2 particles

The properties of nano-SiO2 particles are shown in Table 2.

2.1.3. Aggregates

Locally available natural sand with particles smaller than 0.5mm and fineness modulus of 2.25 and specific gravity of 2.58g/cm3 was used as fine aggregate. Crushed basalt stored in the laboratory with maximum size of 15mm and specific gravity of 2.96g/cm³ was used as coarse aggregate.

2.1.4. Mixture proportioning

A total of two series of mixtures were prepared in the laboratory trials. Series C0 mixtures were prepared as control specimens. The control mixtures were made of natural aggregates, cement and water. Series N were prepared with different contents of nano-SiO2 particles with average particle sizes of 15 nm. The mixtures were prepared with the cement replacement of 0.5%, 1.0%, 1.5% and 2.0% by weight of nano-SiO2 particles. The water to binder ratio for all mixtures was set at 0.40 [5]. The aggregates for the mixtures consisted of a combination of crushed basalt and of fine sand, with the sand percentage of 30% by weight. The binder content of all mixtures was 550kg/m3.  The proportions of the mixtures are presented in Table 2.

2.2. Preparation of test specimens

Series N mixtures were prepared by mixing the course aggregates, fine aggregates and powder materials (cement and nano-SiO2 particles) in a laboratory concrete drum mixer. The powder material in the series C0 mixtures was only cement. They were mixed in dry condition for two minutes, and for another three minutes after adding the water. Slumps of the fresh concrete were determined immediately to evaluate the workability following the mixing procedure. Cubes of 100mm edge were cast and compacted in two layers on a vibrating table, where each layer was vibrated for 10 s [6]. The moulds were covered with polyethylene sheets and moistened for 24h. Then the specimens were demoulded and cured in water at a temperature of 20o C prior to test days. The compressive strengths tests of the concrete samples were determined at 7, 28 and 90 days. The reported results are the average of three trials.

2.3. Compressive strength of nano-SiO2 particles blended concrete

Compressive strength of nano-SiO2 particles blended cement concrete cubes was determined as per ASTM C 39 after 7, 28 and 90 days of moisture curing.

2.4. Workability

Standard slump tests conforming to ASTM C143 were used to determine the workability of the concrete.

3. Experimental results and discussion

3.1. Compressive strength

The compressive strength results of series C0 and N mixtures are shown in Table 3. Comparison of the results from the 28 and 90 days samples shows that the compressive strength increases with nano-SiO2 particles up to 1.0% replacement (N2) and then it decreases, although 1.5% replacement (N3) is still higher than those of the plain cement concrete (C0). It was shown that the use of 2.0% nano-SiO2 particles decreases the compressive strength to a value which is lower than that of control concrete.

This may be due to the fact that the quantity of nano-SiO2 particles present in the mix is higher than the amount required to combine with the liberated lime during the process of hydration thus leading to excess silica leaching out and causing a deficiency in strength as it replaces part of the cementitious material but does not contribute to strength [7]. Also, it may be due to the defect of dispersion that causes weak zones.

The highest enhancement in compressive strength of the N series blended concrete are due to the rapid consuming of Ca(OH)2 which was formed during hydration of Portland cement at early ages that is related to the high reactivity of nano-SiO2 particles. As a consequence, the hydration of cement is accelerated and larger volumes of reaction products are formed. Also nano-SiO2 particles recover the particle packing density of the blended cement, directing to a reduced volume of larger pores in the cement paste.

3.2. Workability

Basically, the bigger the measured height of slump, the better the workability will be, indicating that the concrete flows easily but at the same time is free from segregation [8].

Test results of workability are presented in Figure 1. It shows the influence of nano-SiO2 particles content on the workability of mixtures at constant water to binder ratio of 0.40. Unlike the C0 series, all investigated nano-SiO2 particles blended mixtures had declined workability with high slump values.

4. Conclusion

The results show that the nano-SiO2 particles -blended concrete had higher compressive strength with that of the concrete without nano-SiO2 particles.  It is found that the cement could be advantageously replaced by nano-SiO2 particles up to maximum limit of 1.5% with average particle sizes of 15 nm. Although, the optimal level of nano-SiO2 particles content was achieved with 1.0% replacement. Partial replacement of cement by nano-SiO2 particles decreased workability of fresh concrete.

References:

[1] Sorelli L, Constantinides G, Ulm FJ Toutlemonde F. The nano-mechanical signature of Ultra High Performance Concrete by statistical nanoindentation techniques, Cem Concr Res 2008; 38: 1447–1456.

[2] Sun MQ, Liu QP, Li ZQ, Hu YZ. A study of piezoelectric properties of carbon fiber reinforced concrete and plain cement during dynamic loading. Cem Concr Res 2000; 30: 1593– 1595.

[3] Chung DDL. Cement reinforced with short carbon fibers: a multifunctional material, Composites. Part B 2000; 31: 511 –526.

[4] Naji Givi A, Abdul Rashid S, Aziz FNA, Salleh MAM. Contribution of Rice Husk Ash to the Properties of Mortar and Concrete: A Review. J Am Sci 2010; 6(3): 157-165.

[5] Zivica V. Effects of the very low water/cement ratio. Const Build Mater 2009; 23(8): 2846-2850.

[6] Bui DD, Hu J, Stroeven P. Particle size effect on the strength of rice husk ash blended gap-graded Portland cement concrete. Cem Concr Compos 2005; 27(3): 357–366.

[7] AI-Khalaf MN, Yousift HA. Use of rice husk ash in concrete. Int J Cem Compos Lightweight Concr 1984; 6(4): 241-248.

[8] Lin YH, Tyan YY, Chang TP, Chang CY. An assessment of optimal mixture for concrete made with recycled concrete aggregates. Cem Concr Res 2004; 34(8): 1373-1380.

Figure 1. Effects of particle size of nano-SiO2 particles on workability of concrete.

N1,N2,N3 and N4 are the series N blended concrete with 0.5, 1.0, 1.5 and 2.0 percent of nano-SiO2 particles, respectively.

Table 1

Chemical and physical properties of Portland cement (Wt. %)

Chemical properties

| Material | SiO2 | Al2O3 | Fe2O3 | CaO | MgO | SO3 | Na2O | K2O | Loss on ignition |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Cement | 21.89 | 5.3 | 3.34 | 53.27 | 6.45 | 3.67 | 0.18 | 0.98 | 3.21 |

Specific gravity: 1.7 g/cm3

Table 2. The properties of Nano-SiO2

| Diameter (nm) | Surface Volume ratio (m2/g) | Density (g/cm3) | Purity (%) |
| --- | --- | --- | --- |
| 15 ± 3 | 160 ± 12 | < 0.14 | > 99.9 |

Table 2

Mixture proportion of nano-SiO2 particles blended concretes

| Sample designation | nano-SiO2 particles | Quantities (kg/m3) |
| --- | --- | --- |
|  |  | Cement | nano-SiO2 particles |
| C0 (control) | 0 | 550 | 0 |
| N1 | 0.5 | 547.25 | 2.75 |
| N2 | 1.0 | 544.50 | 5.50 |
| N3 | 1.5 | 541.75 | 8.25 |
| N4 | 2.0 | 539.00 | 11.00 |

Water to binder [cement + RHA] ratio of 0.40, sand 492 kg/m3, and aggregate 1148 kg/m3

Table 3

Compressive strength of nano-SiO2 particle blended cement mortars

|  |  | Compressive strength (MPa) |
| --- | --- | --- |
| Sample designation | nano-SiO2 particle (%) | 7 days | 28 days | 90 days |
| C0 (control) | 0 | 27.3 | 36.8 | 42.3 |
| N1 | 0.5 | 31.6 | 42.7 | 46.5 |
| N2 | 1.0 | 33.1 | 43.6 | 48.1 |
| N3 | 1.5 | 32.2 | 42.9 | 47.7 |
| N4 | 2.0 | 28.5 | 39.7 | 44.3 |

Water to binder [cement + RHA] ratio of 0.40