Determination of Bauxite’s phases by the bomb digest method at Kamsar laboratory ISO 9002 (Guinea)

¶

Ibrahima Sory Cissé, Jiwen Ge*, Lansine Kalifa Keita Vanny Leng

(Institute of Ecology and Environmental Sciences, School of Environmental Studies, China University of Geosciences, Wuhan, 430074, China)

Ibrahima Sory Cissé: Department of Chemistry ,Gamal Abdel Nasser University ,Guinea

Jiwen Ge  :PhD, Professor of Plant Ecology and Conservation Biology China University of Geosciences

Lansine Kalifa Keita Department of Geography , Bamako University , Mali

Vanny Leng :Foot Technology , Cambodge University

Corresponding author: gejiwen2002@yahoo.com.cn

Abstract

This paper presents the results of the experimental work done to find out the extraction percentage of alumina content in ore samples of bauxite from three mines of Guinea .So the knowledge of the chemical composition of a matter or a product directs us on its origins, its possible use and especially towards the technology which it will be necessary to apply for its transformation. ¶This chemical composition is given at the laboratory which, to have reliable results uses adequate methods of analysis for each type of element to be proportioned in the matter.¶ Thus for the analysis of bauxite exploited by the company of bauxites to Guinea (C.B.G.) ¶and which currently comes from the plates of Sangaredi, Bidikoum and Silidara, the chemistry laboratory of Kamsar uses mainly two categories of methods which are  ¶instrumental and wet chemical method (volumetric). This study has relied on the chemical method due that it primarily rests on the quality of the matter to analyze and the concentration of the chemical elements which make it up. To this end, the Guinean bauxite exploited by the C.B.G having a high percentage in Al2O3 and a content of SiO2 not exceeding 7%, for the determination of the various phases from this one, the section bomb digest of the laboratory at Kamsar uses a wet alkaline attack. Under high pressure and at variable temperatures according to the mineralogical phase to determine, this digestion  is schematized as:Al2O3 + 2NaOH  - 2NaAlO2 +H2O. Soluble aluminate. ¶

¶¶¶Key words: Bauxite’s phases, Gibbsite, Boehmite, Guinea and Bomb digests

- Introduction

Initially the bauxite term was introduced in 1821 by the French man Berthier to indicate a red ground deposit level on the ground, close to the village of the Baux - de - Province (valley of Rhone) in the Southern France (Sedat et al. 2006; J.Canérot et al 1999) The term bauxite is used to describe weathering products rich in alumina but low in alkali, alkaline earth and silica. It is composed principally of one or more hydrated aluminum minerals: gibbsite (Al2O3·3H2O), boehmite (Al2O3·3H2O) and diaspore (Al2O3·H2O) with impurities of silica, iron oxide, titanium oxide and other elements in minor or trace amounts (Y. Idris et al.2004 .Shaffer, 1975). Valeton, I., 1972. Bauxites: Development in Soil Science, vol. 1. , Elsevier Publishing Company, Amsterdam.Valeton (1972) defined bauxite ore as bauxite that is economically mineable at present or in the foreseeable future, containing not less than 45–50% Al2O3, and not more than 20% Fe2O3 and 3–5% combined silica.

In terms of the geological field exploration for bauxite, the quantities and topological distribution of the main components and that of the contaminants are of great importance to be reckoned with in the search for new resources. Early international practices of bauxite analyses are usually done to determine loss of ignition, and alumina, silica, iron oxide and titanium contents. But recently, the range of bauxite components considered has been extended to the contaminants, substantially influencing bauxite processing (Authier-Martin et al., 2001; UNIDO, 1985). An idea of the contents of these contaminants is therefore very important as it is taken into account when determining the individual value and price of a given ore.

The world's prospective bauxite resources are located mainly in the developing countries, where one half of the world production comes from (Dash et al., 2007;Lotze, 1978). In Africa, the largest deposits are found in Guinea, which account for Africa's 83.7% proven and probable resources of high-grade bauxite (Y. Idris et al.2004 Church, R.J.H., 1987. Ghana. In: Africa South of the Sahara. Eupa Publications Limited, p. 481.) with Cameron coming second in terms of proven reserve (Clarke, 1987). Other African bauxite producers are Ghana, Mozambique, Sierra Leone and Zimbabwe.The bauxite is a no definite geological formation, ¶it is a mixture of oxides whose aluminum oxide is far more dominating, then comes the iron oxide which gives the reddish color to bauxite, the silica oxide and some compounds from metals such as: ¶vanadium, titanium, lead, calcium, Zinc. ¶Sometimes sulphur, copper, Nickel ,according by M.Karadag et al 2009.

The composition of bauxites generally varies in the following percentages (Santos et al 2004):¶

AL2O3   40-60%;                  H2O 12-30%;                Fe2O3  5-30%;                    SiO2    1-20%

The bauxites quality initially depends on their content of Al2O3 and SiO2. The more the bauxites contain Al2O3 and less SiO2, the higher their economic and industrial values are significant ¶(Tardy et al. 1991).

In Kamsar, it is the trihydrate which is most widespread whose characteristics make this bauxite most economically exploited. ¶ It is most soluble in alkalis and dissolves between 90 at 100 C. It comes in general from the deterioration of the sediments (schist, aleurolothes, argillites) and basic magmatic rocks (dolerites, gabbro-dolerites, konga-diabase) (Luke J. Kirwan 2009).

The bauxite of Guinea exploited by the CBG is in the open air very rich in alumina and a content of SiO2 lower than 7 %( Santos M.C, 2003). For bauxites rich in Al2 O3 and low SiO2, the wet alkaline process is best according by N. Zwingmann et al 2009 .The purpose of this study therefore is to ascertain the quality and the nature of bauxite often the customers’ request.¶

Compared to the other methods of decomposition and setting in solution such as the triacid method (HCI, HNO3 and H2SO4), this method uses little reagent, less expensive, less toxic, gives reliable and precise results (S.A. Hussain et al. 2000). ¶

One of the sections in the kamsar’s laboratory use this method which calls section Bomb digest.

II - Properties of alumina hydrates

The properties of alumina hydrate (A. Asghar Calagari, 2007) as fallowing :(Table 1)

III - Method and Materials

III.1- Materials and solutions needed

This study has used the following materials (Table 2)

Solutions Needed

1. NaOH standard solution (CNaOH=0.500 mol/L)                6. NaCl 5 g/l              11. KF solution

2. HCl standard solution (CHCl=0.500 mol/L)                       7. NaOH 102g/l

3. NaOH.SiO2) 102 g/l                                                           8.Phenolphthalein indicator ¶

4.¶Starch and paper pulps                                                       9. Buffer solution pH 8.0

5. Gluconate of sodium (NaC6H11O7  )                                                              10. HCl1:1 solution

III.2- Methods used

The quantity (1,3±0,0001g and  0,65±0,0001g) of bauxite are heated, under pressure, in a solution of sodium hydroxide (102g/l) respectively at 143°C , 235°C (fig.1); the insoluble matters are separated by filtration. A alumina present in the filtrate is given by titrating the equivalent of the ions hydroxides (OH -) released by fluorine in a chelating solution containing sodium gluconate (Loh et al., 2005). ( Figure 1)

The Chemical Processes involving the dissolution of Al2O3 by soda is done according to the reaction below:

Al2O3 +2NaOH – 2NaAlO2 + H2O (eq.1)

A part of Al2O3 and SiO2 combined in kaolinite reacts on soda according to the equation (eq.2)

Al2O3.2SiO2 +H2O +2NaOH – Na2O.Al2O3.2SiO2 +2H2O           (2)

The starch and paper pulp make it possible to agglomerate the fine suspended particles in the bomb and to release the base with the policeman from it. The sodium gluconate (NaC6H11O7 or CH2OH-(CHOH)4C=o-ONa in solution 25% combines with sodium aluminates to form a complex easily hydrolysable as shown in equation 3.

NaAlO2 +CH2OH-(CHOH) 4-C=oONa + 2H2                 Al (OH)3+CH2OH-(CHOH)4  C=oONa  + NaOH (3)

The KF solution moves sodium gluconate to fix aluminum in the form of cryolite (Santos et al 2004a) (eq.4). ¶

Al(OH)3 +CH2OH (CHOH)4-C=oONa + 6KF       AlF6 K3 +CH2OH-(CHOH)4-C=oONa + 3KOH  and the potash releases which one titrates by HCI 0.5 normal by using at the same time the pHmeter and the indicator according to the equation 5.

KOH +  HCI                KCI + H2O where  H+ +OH-                 H2O (eq.5)

III.2.1- Determination of alumina by the equations of the reactions ¶

Adding equations 1,3 and 4 by multiplying the two last by 2 to obtain the general equation of proportioning

Al2O3 + 2NaOH       2NaAlO2 + H2O

2NaAlO2+2CH2OH-(CHOH)4-C-ONa+4H2O          2Al(OH)3+CH2OH(CHOH)4-C-ONa + 2NaOH

2Al (OH)3+CH2OH(CHOH)4-C-ONa+12KF             2K3AlF6 + 2CH2OH-(CHOH)4-C-ONa + 6KOH

Al2O3 + 12KF + 3H2O                  2K3AlF6 + 6KOH (eq.6)

KOH + HCl                   KCl + H2O

where      OH- + H+    ↔   H2O

Equation (5) is a reaction of neutralization and at equivalence we have: ¶quantity of ions OH - released by the solution of KOH is equal to that of the ions H + brought by the solution of HCl  0.5 N. ¶

nOH- = nH+ →NOH- × VOH- = N H+ × VH+  =  meg

According to the formula mass m = Eq.meg → meg = m / Eq = NOH- × VOH- = N H+ × VH+

And the equation of reaction, we obtain

NOH- × VOH- = N H+ × VH+ = mKOH / EqKOH → mKOH = N H+ × VH+ × EqKOH-

From equation (6)

102g Al2O3 → 6 × 56g KOH

mAl2O3 → mKOH

x m  mAl2O3 = 102g χ mKOH / 6 x 56g = 102xNH + VH + x EqKOH / 6x56g

EqKOH = 56/1 =56 ; N H+ = 0.5N

mAl2O3 = 102g x 56 x NH+ x VH+ / 6 x 56g = 102 x 0.5 / 6 x VH +

mAl2O3 = 8.5  VH + en mg.

In practice, we checked if all the quantity of KOH is proportioned by adding 5ml HCl 0.5 N in excess which we titrated by soda having same normality.

Not proportioned KOH is equal to 5 - VNaOH  ¶where  ¶mAl2O3 = 8.5  × 10-3(VH+ + 5 – VNaOH) in gram but VNaOH  + 5 = VTHCl therefore mAl2O3 = 8.5  × 10-3(VTHCl – VNaOH).

Knowing the mass of Al2O3,we determined its percentage according to the relation

PE→ 100

mAl2O3 → y    ;    y = (mAl2O3 / PE) × 100

y = % Al2O3 = (8.5 × 10-3(VTHCl – VNaOH)/PE) × 100

In the furnace of 143°C PE = 1.3±0. 0001

% Al2O3 = 0.85 (VTHCl – VNaOH) / 1.3.      % Al2O3 = 0.65(VTHCl – VNaOH)

In the furnace of 235°C PE = 0.65± 0.0001

% Al2O3 = 0.85 (VTHCl – VNaOH) / 0.65.   % Al2O3 = 1.3(VTHCl – VNaOH)

III.2.2- Mass percentage of Al2O3

Formula: % Al2O3 (gibbsite) = (axV±b/1.30) × x100

% Al2O3 (gibbsite and boehmite) = (axV±b/0.65) × x100

Factor of the day: y = 0.00891x – 0.0114

IV- Results and Discusions

The concentration of Al2O3 (143°C) and Al2O3 (235°C)  in the samples as presented respectively in Table 3 ranges from 44.43% to 44.49% ;Table 4 ranges from 50.33% to 50.34% . For the standard bauxite sample N°021002040s the analyzed concentration of Al2O3 (143°C)as presented below in Table 3 is 44.83% as compared to the certified value of 44.77%; inTable 4 is 51.84% as compared also to the certified value 51.84 This shows that the error in terms of accuracy of the measurement is less than 1%. Also the error in terms of precision of the measurements defined as one standard deviation of the percentage of the mean is less than 2% for all the samples.(Table 3) and (Table 4).

From table (3) and (4),the experiment  showed that trihydrate (gibbsite) is more soluble than monohydrate (boehmite). ¶It dissolves at lower temperatures but in the solution, it is transformed into monohydrate at high temperature

The results show that solubility increases with the soda concentration used and the temperature. ¶This is why in the bomb digest, trihydrate is attacked at 143°C and at the temperature of 235°C we have the two (2) phases which are attacked (H. Chuanbin et al 2008)  ¶.The advantage of these proportioning results from the request of the customers for whom the choice of quality depends on the nature of bauxite, ¶otherwise if  the bauxite is a monohydrate or a tri hydrate

By P. Smith 2009, the bauxites with weak content of SiO2 are the best on the market; because in the current industry of Al2O3, the most delicate operation is the separation of impurities containing silica. ¶

V- Conclusion

This study briefly focused on the section bomb digest of chemistry laboratory , to define the types of bauxite and especially the contents of Al2O3 soluble.

The determination of the bauxite mineralogical phases by the Bomb digest method makes it possible to know well the nature of bauxite and especially its content of soluble Al2O3, i.e. the decompositions at the temperature:¶  143°C pour le trihydrate (gibbsite)  and 235°C for total alumina (trihydrate and monohydrate).

The chemical composition in Al2O3 soluble is significant, but it is also necessary to lay a particular stress on the method of proportioning for the bomb digest which for the moment is used. The method of the calibration curve can show the impossibility of measurement in consequence of awkward substances, if a line is not obtained, in this case it is recommended to use the chemical reactions for the calculation of the percentage of Al2O3.

VI-References

[1] A. Asghar Calagari and A. Abedini, 2007.Geochemical investigations on Permo-Triassic bauxite horizon at Kanisheeteh, east of Bukan, West-Azarbaidjan, Iran Journal of Geochemical Exploration 94 (1-3) 1-18

[2] Authier-Martin et al., 2001 M. Authier-Martin, G. Forté, S. Ostap and J. See, the mineralogy of bauxite for producing smelter-grade alumina, Journal of the Minerals, Metals and Materials Society 53 (2001), pp. 36–40

[3] Clarke, J.I., 1987. Cameron. In: Africa South of the Sahara. Eupa Publications Limited, p. 303. [4] Dash et al., 2007 B. Dash, B.C. Tripathy, I.N. Bhattacharya, S.C. Das, C.R. Mishra and B.S. Pani, Effect oftemperature and alumina/caustic ratio on precipitation of boehmite in synthetic sodium aluminate liquor, Hydrometallurgy 88 (2007), pp. 121–126.

[5] F.Vitali et al 2001.Hydrogen-isotope fractionation in aluminum hydroxides: Synthesis products versus natural samples from bauxites 65(9) 1391-1398

[6] Funtua, I.I., 2001. Elemental composition of sn–Nb–Ta mine tailings of Jos Area, Central Nigeria. Chem. Erde 61, pp. 45–53.

[7] Huang Chuanbin and Wang Yuhua 2008.Removal of aluminosilicates from diasporic-bauxite by selective flocculation using sodium polyacrylate. Elsevier journal 59(3) 299-303.

[8] J.Canérot et al  1999 .Stratigraphic and geodynamic setting of alterites and bauxites on the Iberian Margin of the Western Pyrenees (France) Elsevier journal 328(7) 451-456

[9] Loh et al., 2005 J. Loh, C. Vernon, M. Loan and G. Brodie, Boehmite vs. gibbsite precipitation, Light Metals 2005 (2005), pp. 203–208

[10] Lotze, J., 1978. Economic Evaluation of world's Bauxite Resources. Proceedings of the fourth International Congress ICSOBA, Athens, National Techn University of Athens, 2, p. 494.

[11] Luke J. Kirwan 2009 Characterisation of various Jamaican bauxite ores by quantitative Rietveld X-ray powder diffraction and 57Fe Mössbauer spectroscopy International journal of Mineral processing 91(1-2) 14-18

[12] M.Karadag et al 2009 Rare earth element (REE) geochemistry and genetic implications of the Mortaş bauxite deposit (Seydişehir/Konya – Southern Turkey) .Chimie der Erde Geochemistry 69(2) 143-159

[13] N. Zwingmann et al., 2009. A method to concentrate boehmite in bauxite by dissolution of gibbsite and iron oxides .Elsevier journal 97(1-2) 80-85

[14] P. Smith, 2009 .The processing of high silica bauxites - Review of existing and potential processes. Elsevier journal. 98(1-2) 162-176.

[15] S.A. Hussain and R. Jamal, 2000. Evaluation of an HCl process for leaching of low-grade highly siliceous bauxite ore. Oral Session, Proceedings of the XXI International Mineral Processing Congress, 13, C6-8-C6-14

[16] Santos, M.C., Varajao, A.F.D.C., 2004. Sedimentation and pedogenic features in a clay deposit in Quadrila´tero Ferrı´fero, Minas Gerais, Brazil. Anais da Academia Brasileira de Cieˆncias 76, 147– 159.

[17] Santos, M.C., Varaja˜o, A.F.D.C., Yvon, J., 2004a. Genesis of clayey bodies in Quadrila´tero Ferrı´fero, Minas Gerais, Brazil. CATENA 55 (3), 277– 291.

[18] Santos M.C., 2003. Caracterizac¸a˜o dos depo´ sitos argilosos na porc¸a˜o centro-sul do Sinclinal da Moeda, Quadrila´tero Ferrı´fero, MG,Brasil: macromorfologia, micromorfologia, cristaloquVmica, geˆnese e considerac¸o˜es industriais

[19] Sedat Temur and Gürsel Kansun ,2006.Geology and petrography of the Masatdagi diasporic bauxites, Alanya, Antalya, Turkey .Journal of Asian earth Sciences 24(4) 512-522.

[20] Shaffer, J.W., 1975. Bauxite raw materials. In: Industrial Minerals and Rocks (Non-metallic other than Fuels). Amer Inst Mining Metall Petroleum Engineering. Inc., 442–459

[21] Tardy, Y., Kobilsek, B., Parquet, H., 1991. Mineralogical composition and geographical distribution of African and Brazilian periatlantic laterites. The influence of continental drift and tropical paleoclimates during the past 150 million years and implications for India and Australia. Journal of African Earth Sciences 12, 283– 295.

[22] UNIDO, 1985. Bauxite testing laboratories. Development and transfer of technology series, 20 (ID/316/Abstract).

[23] Valeton, I., 1972. Bauxites: Development in Soil Science, vol. 1. , Elsevier Publishing Company, Amsterdam.

[24] Y. Idris, I. I. Funtua and I. M. Umar. 2004, Rapid analysis with energy-dispersive X-ray fluorescence spectrometry for bauxite investigation on the Mambilla Plateau, North Eastern Nigeria .Elsevier journal 64(4) 385-398.

Tables Captions

Table 1: The Properties of alumina hydrates

Table 2: materials and specifications

Table 3: Quantity of gibbsite contained in each 1,3±0,0001g of bauxite samples at 143°C

Table 4: Quantity of gibbsite and boehmite contained in each 0,65±0,0001g of bauxite samples at 235°C

Figure Caption

Figure 1: The furnaces of 143°C and 235 °C

.Table1

| N° | Designation | Gibbsite or Hydrargillite | Boehmite | Diaspore |
| --- | --- | --- | --- | --- |
| 1 | Content alumina | 65.4 | 85 | 85 |
| 2 | System Crystallin | Monoclinic | Orthorhombic | Orthorhombic |
| 3 | Mohs hardness | 2.5-3.5 | 3.5-4.0 | 6.5-7.0 |
| 4 | Fast temperature of dehydration | 150°C | 350°C | 450°C |
| 5 | Product of dehydration | X-Al2O3 | Y-Al2O3 | Z – Al2O3 |
| 6 | Density | 2.42 | 3.01 | 3.44 |
| 7 | Solubility in Na2O 100g/l à 125°C, Al2O3 g/l | 128 | 54 | unsoluble |

Table 2

| N° | Materials | Specifications |
| --- | --- | --- |
| 1 | Thermometer | control the temperature |
| 2 | Whattman 40 | filter the solution |
| 3 | Bombs | in which is the bauxite-soda mixture |
| 4 | Furnaces of 143C and 235C | allow heating the bomb containing the mixed solution (bauxite-soda) |
| 5 | Copper disc | for the bomb |
| 6 | Drying oven 105C | dry bauxite ¶ |
| 7 | Torque wrench | tighten the lid of the bomb firmly |
| 8 | Burette and stand | for the titration |
| 9 | Bomb pilot | for the control |
| 10 | Sound stop watch | for the time |
| 11 | Grip | leave the bombs in the furnaces |
| 12 | Bain-marie | cool the bombs |
| 13 | Policeman | : in which we put water to clean the bombs |
| 14 | Magnetic stirrer | make homogeneous the solution |
| 15 | Cone cup 500ml | in which the mixture occurs |

Table3

| N° Bomb | N° of Laboratory | Mass samples | Calculation | %Mass |
| --- | --- | --- | --- | --- |
| 06 | 021002035 | 1.3000 | 65.70 + 5 =70.70-4.50 = 66.20 | 44.49 |
| 12 | 021002036 | 1.3000 | 65.80 + 5 =70.80-4.50 = 66.30 | 44.56 |
| 13 | 021002037 | 1.3000 | 65.60 + 5 =70.60-4.50 = 66.10 | 44.43 |
| 14 | 021002038 | 1.3000 | 65.70 + 5 =70.70-4.50 = 66.20 | 44.49 |
| 15 | 021002040s | 1.3000 | 66.10 + 5 =71.10-4.50 = 66.60 | 44.77 |
| 16 | 021002040s | 1.3000 | 66.20 + 5 =71.10-4.50 = 66.70 | 44.83 |

Table 4

| N° Bomb | N° of Laboratory | Mass samples | Calculation | %Mass |
| --- | --- | --- | --- | --- |
| 17 | 021002035 | 0.6500 | 37.60 + 5 =42.60-4.60 = 38.0 | 50.34 |
| 18 | 021002036 | 0.6500 | 37.40+ 5 =42.40-4.60 = 37.80 | 50.34 |
| 19 | 021002037 | 0.6500 | 37.60 + 5 =42.60-4.60 = 38.00 | 50.33 |
| 20 | 021002038 | 0.6500 | 37.60 + 5 =42.6 -4.60 = 38.00 | 50.34 |
| 24 | 021002040s | 0.6500 | 38.60 + 5 =43.60-4.50 = 39.10 | 51.84 |
| 25 | 021002040s | 0.6500 | 38.60 + 5 =43.60-4.50 = 39.10 | 51.84 |

Figure 1