Biodegradability of polyethylene by Bravibacillus, Pseudomonas, and Rhodococcus spp.

Author and corresponding author:

Sonil Nanda

Senior Research Fellow

Orissa University of Agriculture & Technology,

Bhubaneswar 751 003, Orissa, India

Mailing address:

Mini Mahal, 											         Haripur Patna, Near Kapileswar High School, 							         Old Town, Bhubaneswar 751 002, Orissa, India					      	                     Cell: +91 9937444333								                                  Email: isonil@yahoo.co.in

Biodegradability of polyethylene by Bravibacillus, Pseudomonas, and Rhodococcus spp.

Sonil Nanda†

Orissa University of Agriculture & Technology, Bhubaneswar 751 003, Orissa, India

†Author for correspondence. Email: isonil@yahoo.co.in

Abstract: The current article investigates the biodegradation ability of Bravibacillus, Pseudomonas, and Rhodococcus spp. in degrading polyethylene. Shake-flask incubation for 3 weeks was performed for the purpose of biodegradation. The initial and final dry weights of polyethylene before and after incubation were compared and the percentage of degradation was calculated. Pseudomonas was found to be most efficient in degrading polyethylene with its biodegradability of 40.5% followed by Bravibacillus with 37.5% and Rhodococcus with 33% biodegradability, respectively.

Key words: Polyethylene, Bravibacillus, Pseudomonas, Rhodococcus, Shake-flask incubation, Biodegradation

- Introduction:

Polyethylene is a polymer made up of long chain monomers of ethylene. It is a thermoplastic commodity mostly used for packaging. The worldwide utility of polyethylene is expanding at a rate of 12% per annum and approximately 140 million tonnes of synthetic polymers are produced worldwide each year (Shimao, 2001). With such huge amounts of polyethylene getting accumulated in the environment, their disposal evokes a big ecological issue. It takes thousand years for their efficient degradation. The durability, light weight, and processability of polyethylene causes it to linger in the nature for centuries and end up in landfills and/or natural water resources (Jang et al., 2002). Although there has always been a search for efficient disposal of polyethylene yet the biological means holds certain concern other than the chemical modes. Some possible measures employed for the purpose are biodegradation and biorecycling (Yang et al., 2005). Recycling is not economically feasible due to cost and loss of mechanical properties (Yang et al., 2004). However, biodegradation serves a tangible alternative.

Amongst the biological ways, microbial biodegradation is widely accepted and is still underway for its enhanced efficiency. Microbial degradation of plastics is caused by certain enzymatic activities that leads to a chain cleavage of the polymer into oligopolymers and monomers. These water soluble enzymatically cleaved products are further absorbed by the microbial cells where they are metabolized. Aerobic metabolism results in carbon dioxide and water (Starnecker and Menner, 1996) where as anaerobic metabolism results in carbon dioxide, water, and methane as the end products, respectively (Gu et al., 2000). The degradation leads to breaking down of polymers to monomers creating an ease of accumulation by the microbial cells where they undergo biodegradation. The depolymerisation results due to various physical or biological forces (Swift, 1997). The physical forces such as temperature, moisture, pressure etc. deal with causing mechanical damage to the polymer so that the biological forces like the enzymes catalyze the process.

This research article focuses on the biodegradation of polyethylene by Bravibacillus, Pseudomonas, and Rhodococcus spp. by pure culture shake-flask incubation method. The percent of biodegradation was evaluated by comparing the initial and final dry weights of polyethylene before and after incubation. The hypothesis of the study was microorganisms will utilize polyethylene as the sole source of carbon and energy in the medium when the rest of the nutrients are limited.

- Materials and Methods:

  - Isolation of Polyethylene Degrading Bacteria

Bravibacillus, Pseudomonas, and Rhodococcus spp. were isolated from a soil sample collected from a polyethylene-waste disposal site and obtained in pure cultures to be used as the inoculum in degrading polyethylene.

  - Pre-treatment of Polyethylene

General grade polyethylene for commercial grocery purpose was used to investigate its biodegradability nature. The polyethylene was cut into small and fine pieces, washed with ethanol (to remove the organic matter adhering to the surface of polyethylene) and distilled water, and air-dried. The pieces were taken in a mortar pestle along with sufficient amount of crystalline NaCl and were ground till they get minced in form of fine ruptured threads. The mixture was transferred into a conical flask with distilled water and mixed well in a shaker for 1 hour. Crystalline NaCl was chosen for the purpose because the crystals would help in easy grinding and rupturing the sheets and its solution would wash away all impurities and organic matter adhering to it. The solution was passed through Whatman no. 41 filter paper. Polyethylene particles were recovered from over the filter paper gently and air-dried.

  - Treatment of Polyethylene

The isolated Bravibacillus, Pseudomonas, and Rhodococcus spp. were individually inoculated in 100 ml of nutrient broth taken in conical flasks. 0.2 g of the polyethylene particles were amended to each flask except the control. Thus the experimental set up gave three designs T1 (polyethylene + Bravibacillus), T2 (polyethylene + Pseudomonas), and T3 (polyethylene + Rhodococcus). All the treatments were incubated in an incubator shaker at 150 rpm for 3 weeks but due to variation in growth temperatures, T1 was incubated at 50°C where as T2 and T3 at 40°C, respectively. The experiments were conducted in triplicates with a control and blank.

  - Dry Weight Determination of Recovered Polyethylene

The residual polyethylene particles were recovered from the broth cultures by passing though a course filter paper. The bacterial biofilm adhering to the polyethylene surface was washed by a 2% (v/v) aqueous sodium dodecyl sulphate solution for 3 to 4 hours and finally with distilled water. The washed polyethylene particles were air-dried and weighed. The dry weights of recovered polyethylene from the culture media were taken in weekly intervals (i.e. day 0, day 7, day 14, and day 21) for accounting the rate of biodegradation.

- Results and Discussion:

After incubation, the culture flasks were removed from the incubator shaker and tested for the viability of microorganisms and any contamination in the medium. The test results indicated a good stability of the three bacteria in the medium with no sign of contamination. Biofilm formation by the three bacteria was clearly visible in the broth and that of Pseudomonas was too viscous and slimy.

Table 1. Comparative analysis of the polyethylene weights in different treatments before and after incubation

| Treatments | Amount of polyethylene (g) | Amount of polyethylene degraded (g) | Percentage of degradation |
| --- | --- | --- | --- |
|  | Initial | Final |  |  |
| Control | 0 | 0 | 0 | 0 |
| Blank | 0.2 | 0.2 | 0 | 0 |
| T1 | 0.2 | 0.125 | 0.075 | 37.5 |
| T2 | 0.2 | 0.119 | 0.081 | 40.5 |
| T3 | 0.2 | 0.134 | 0.066 | 33.0 |

A comparative analysis of polyethylene biodegradation within the treatments has been shown in Table 1. Out of the three treatments, T2 (polyethylene + Pseudomonas) gave the best biodegradability of 40.5% followed by T1 (polyethylene + Bravibacillus) which gave 37.5%, and 33% by T3 (polyethylene + Rhodococcus), respectively.

During the 3 weeks incubation, the system was maintained undisturbed with no addition or removal of nutrients to and from the medium. Hence, it might be assumed that when the basal nutrients from the media were entirely utilized by the bacteria, polyethylene acted as the readily available source of carbon and energy. Figure 1 shows the rate of biodegradation by Bravibacillus, Pseudomonas, and Rhodococcus taken in weekly intervals for 3 weeks. The trend for T2 appeared slightly zig-zag because initially in the first week Pseudomonas would have taken a longer time in adapting to the changing environments but during the second and the third week a boost in the biodegradation rate is found which suggests that this would have been possible for the enhanced biofilm formation and enzyme activities on polyethylene particles.

Figure 1. Trend of biodegradation of polyethylene in different treatments

Biodegradation depends upon polymer characteristics, organism type and nature of pre-treatment (Shah et al., 2008). The pre-treatment of polyethylene is very significant for its biodegradation. Physical rupturing of the polyethylene and chemical washing by ethanol might have added value to its degradability. To support this, Volke-Sepulveda et al. (2002) showed that addition of ethanol to fungal cultures containing polyethylene improved the biodegradation of polyethylene. Despite the fact that the isolated bacteria were native to the site of polyethylene disposal and might show some degradability in natural conditions, yet they also exhibited biodegradation in laboratory conditions on synthetic media. This gives some clue that these bacteria can be used in both natural and artificial conditions for the purpose of degradation of polymers.

Although there has been growing explorations in degrading polyethylene, yet the fate of these organic polymers in the environment and the time required for their complete mineralization to carbon dioxide needs to be fully understood (El-Shafei et al., 1998).  However, the interest of research still lies in examining the activity of a consortium of microorganisms on biodegradation of polyethylene.

- References

El-Shafei HA, El-Nasser NHA, Kansoh AL, Ali AM. Biodegradation of disposable polyethylene by fungi and Streptomyces species. Polymer Degradation and Stability1997;62:361-365.

Gu JD, Ford TE, Mitton DB, Mitchell R. Microbial corrosion of metals. The Uhlig Corrosion Handbook. 2nd Edition. Wiley, New York, USA. 2000:915-27.

Jang J-C, Shin P-K, Yoon J-S, Lee I-M, Lee H-S, Kim M-N. Glucose effects on the biodegradation of plastics by compost from food garbage. Polymer Degradation and Stability 2002;76:155-159.

Shah AA, Hasan F, Hameed A, Ahmed S. Biological degradation of plastics: A Comprehensive review. Biotechnology Advances 2008; 26:246-265.

Shimao M. Biodegradation of plastics. Current Opinion in Biotechnology 2001;12:242-247.

Starnecker A, Menner M. Assessment of biodegradability of plastics under stimulated composting conditions in a laboratory test system. International Biodeterioration and Biodegradation 1996;85-92.

Swift G. Non - medical biodegradable polymers: environmentally degradable polymers. Handbook of biodegradable polymers. Harwood Acedemic, Amsterdam. 1997:473-511.

Volke-Sepulveda T, Saucedo-Castaneda G, Gutierrez-Rojas M, Manzur A, Favela-Torres E. Thermally treated low density polyethylene biodegradation by Penicillium pinophilum and Aspergillus niger. Journal of Applied Polymer Science 2002; 83,305-314.

Yang H-S, Yoon J-S, Kim M-N. Dependence of biodegradability of plastics in compost on the shape of specimens. Polymer Degradation and Stability 2005;87:131-135.

Yang H-S, Yoon J-S, Kim M-N. Effects of storage of a mature compost on its potential for biodegradation of plastics.  Polymer Degradation and Stability 2004;84:411-417.

Sonil Nanda

Manuscript submitted on 25-02-2010